| Trade of Plumbing |
| --- |
| Module 1: | Thermal Process and Mild Steel Pipework |
| Unit 6: | Mild Steel Pipe Reparation and Jointing |
|  | Phase 2 |

Table of Contents

List of Figures	4

List of Tables	5

Document Release History	6

Module 1 –Thermal Process and Mild Steel Pipework	7

Unit 6 – Mild Steel Pipe - Preparation and Jointing	7

Learning Outcome:	7

Key Learning Points:	8

Training Resources:	8

Exercise:	9

Key Learning Points Code:	9

Mild Steel Pipe & Fittings	10

Mild Steel Pipe Identification	10

Mild Steel Pipe Identification	12

Mild Steel Pipe Assembly	14

Mild Steel Pipe Cutting	15

Thread Cutting	16

Mild Steel Pipe Cutting	18

Thread Cutting	19

Water	20

Maximum Density	21

Water Expansion	23

Specific Gravity	24

Specific Gravity of Materials	24

Self Assessment	26

Index	28

# List of Figures

Figure 1.	Pipe Grades	11

Figure 2.	Mild Steel Pipe Identification	12

Figure 3.	Malleable Pipe Fitting Threads	13

Figure 4.	Iron Tees	13

Figure 5.	Z Dimension	13

Figure 6.	Mild Steel Pipe Assembly	14

Figure 7.	Hacksaw Blade	15

Figure 8.	Pipe Cutters	15

Figure 9.	Pipe Reamer	16

Figure 10.	Thread	16

Figure 11.	Stocks and Dies	17

Figure 12.	Longscrew Connector and Barrel Nipple	17

Figure 13.	Mild Steel Pipe Cutting	18

Figure 14.	Thread Cutting	19

Figure 15.	Water Density	22

Figure 16.	Expansion of Water	23

Figure 17.	Unit Exercise/Procedure No. 2.1.8.A	25

Figure 18.	Identify fittings diagram	27

# List of Tables

# Document Release History

| Date | Version | Comments |
| --- | --- | --- |
| June 2006 | V.1.0 |  |
| 04/03/14 | 2.0 | SOLAS transfer |

# Module 1 –Thermal Process and Mild Steel Pipework

## Unit 6 – Mild Steel Pipe - Preparation and Jointing

Duration – 25 Hours

### Learning Outcome:

By the end of this unit each apprentice will be able to:

State the different sizes, grades of mild steel pipe and their applications.

Describe the types of jointing methods and fittings used for mild steel pipe.

Describe the various tools used in preparation and jointing of mild steel pipe.

Cut and deburr mild steel pipe using hacksaw/pipecutter and pipe reamer.

Thread mild steel pipe using manual stocks and dies.

Change and clean dies in manual stocks and dies.

Assemble mild steel pipework projects.

Describe the physical and chemical properties of water.

Calculate volume and capacity of pipes, cylinders and tanks.

Pressure test mild steel pipework projects using manual test pump.

### Key Learning Points:

| Rk | Mild steel pipe sizes and grades. |
| --- | --- |
| Rk | Fittings and jointing methods. |
| Rk | Mild steel pipefitting tools. |
| Sk H | Use of hacksaw, pipecutter, reamer, stocks and dies. |
| Rk Sk | Correct thread length. |
| H | Thread swarf, oil. |
| Sk | Application of flax, sealing compounds. |
| Sk | Jointing and assembling mild steel pipe. |
| Rk | Preparation of materials list. |
| P | Communication, planning. |
| Sk M | Measurements, tolerances. |
| Sk | Interpretation of drawings. |
| Sk | Bracketing and levelling pipework. |
| P | Working independently, good working practice. |
| Sk | Changing and cleaning dies Sk. |
| Sk | Care of pipefitting tools. |
| Sc | Physical and chemical properties of water, maximum density, relative density etc. |
| M | Calculations of volumes and capacities. |
| Sk | Setting up manual test pump. |

### Training Resources:

Classroom facilities, information sheets, workshop facilities, sample mild steel pipe, fittings, jointing compounds and tools.

### Exercise:

Apprentice to answer sample questions:

Assemble mild steel pipework projects 2.1.6a, 2.1.6b, 2.1.6c and 2.1.6d, in the curriculum document.

Pressure test mild steel projects 2.1.6a, in the curriculum document.

### Key Learning Points Code:

M = Maths	           D= Drawing     RK = Related Knowledge Sc = Science

P = Personal Skills	Sk = Skill	   H = Hazards

# Mild Steel Pipe & Fittings

Mild steel pipe, also known as low carbon steel pipe, is available either painted black or galvanised.  Black steel pipes should be used for hot water heating systems and gas supplies only.  If it were used where freshwater is continuously being drawn off through the pipeline it would soon become liable to corrosion problems.

Steel tube for water and gas services is usually joined by means of screwed joints or by welding.  Galvanised tube, however, must not be welded as the heat would remove the zinc coating and leave the steel unprotected against corrosion attack.  There is also a health risk, in that, when galvanised pipe is heated it gives off fumes that can be injurious to health.  It should be noted that all welding processes produce fumes and care must be taken to minimise exposure to this hazard.

A comprehensive range of pipe fittings as available both for screwed and welded joints, the latter type having no threads but the outer edge bevelled to provide the necessary joint preparation.

## Mild Steel Pipe Identification

Mild steel piping is supplied in 6.4m lengths. Finished in Black or hot dipped galvanised for extra corrosion resistance.

These lengths can have either:

A.  PLAIN ENDS: When they are to be welded together on site.

or

B.  THREADED ENDS: When threaded joints are to be used on site.

On threaded lengths, one socket is supplied with each length.

Mild steel pipes are sized by their internal diameters or bores and come in the following sizes, all in mm.

8, 10, 15, 20, 25, 32, 40, 50, 65, 80, 100, 150, 200 etc.

Mild steel pipes are supplied in different grades for different applications: -

MEDIUM GRADE: Marked with blue band. Suitable for low pressure hot water heating and gas installations.

HEAVY GRADE: Marked with a red band. Suitable for steam and high temperature hot water heating installations.

SCHEDULE 40 & 80: The particular schedule is stamped on the outside of the pipe. These are very heavy walled pipes and are used in process industries.

Actual size:

Pipe Grades

# Mild Steel Pipe Identification

Mild Steel Pipe Identification

The threads on malleable iron pipe fittings are referred to as either male or female. The male thread is the one where the threads are external and visible. The female thread is the one where the threads are internal and hidden.

Malleable Pipe Fitting Threads

When ordering malleable iron tees with unequal outlets quote the size in the order shown in the figure opposite. So the correct way to quote the tees piece shown is: 25mm  X 15mm  X 20mm.

Iron Tees

The Z dimension is the distance from the centre of the fitting to the point reached by the end of the pipe when it has been screwed the proper distance into the fitting.

When piping runs are being prefabricated it is essential to know this dimension and it can be obtained from the fitting manufactures catalogue.

Z Dimension

## Mild Steel Pipe Assembly

Mild Steel Pipe Assembly

Thread seals and taps are always applied in a clockwise direction when facing the threaded end of the pipe.

Polishing brass and chrome plated threads such as radiator valve tailpieces and bib taps may need to be slightly serrated with a hacksaw blade to give the flax or thread tape a grip.

If this is not done the flax of tape will move along the threads as the fitting is tightened leaving none in the joint and probably causing the joint to leak.

BOSS WHITE AND FLAX:

Is suitable for hot and cold water services and low pressure hot water heating.

P.T.F.E TAPE:

Is suitable for all the above mentioned applications as well as joints on oil and gas lines and oxygen and acetylene.

STAG JOINTING COMPOUND:

Is especially suitable for oil and gas lines.

## Mild Steel Pipe Cutting

The teeth on a hacksaw blade are set at a slight angle to enable the blade to produce a cut wide enough so that the rest of the blade does not bind or break.

It is important that the hacksaw blade being used is suitable for the type of material being cut.

Hacksaw Blade

For rapid cutting of mild steel pipes a pipe cutters is used.  It consists of cutting wheel, two guide rollers and an adjusting screw.  The cutting wheel should be replaced periodically as a blunt wheel tends to crush rather than cut the pipe.

Pipe cutters with three cutting wheels are available for applications where the cutters can not be turned completely around by the pipe.

Pipe Cutters

A pipe reamer is used to remove the internal burr left by the pipe cutter.

If this burr is not removed it causes an increased restriction to the flow of water in the pipeline.

Pipe Reamer

## Thread Cutting

The type of thread normally used for connecting mild steel pipes is called a British Standard Pipe Thread or B.S.P.T.

Thread

To cut threads on mild steel pipes a “stocks and dies” is used. This consists of a set of four dies in a holder. This holder fits into a ratchet stock which is fitted with a handle.

Stocks and Dies

To cut a longscrew thread the normal thread cutting procedure is continued until the backnut and socket can be threaded completely on to the pipe.

Barrel nipples can be cut with a special attachment on the electric powered threading machine.

Longscrew Connector and Barrel Nipple

## Mild Steel Pipe Cutting

Mild Steel Pipe Cutting

## Thread Cutting

Thread Cutting

# Water

Pure water is a transparent, tasteless and odourless liquid.

It is a chemical compound composed of two parts hydrogen and one part oxygen (H2 O) and exists as a vapour, liquid or solid depending upon the pressure and temperature it is exposed to.

Water is essential to all forms of life and is generally classified as being either hard or soft.

Water has height, but this varies according to its temperature.  This fact is important in the design and installation of plumbing and central heating systems.  For example, it may effect the placing of taps, for the weight of the water combined with its height above the tap will affect the rate of flow.

For normal everyday purposes, and for simple calculations of forces and pressures, the weight of water is taken to be 1,000kg / m².

The following points are also worth noting:

One litre weighs 1,000 grammes (g).

There are 1,000 litres in 1 m³.

One m³ of water weighs one tonne.

Characteristics of water:

Characteristics of Water

| Boiling point | 100ºC |
| --- | --- |
| Freezing point | 0ºC |
| Maximum density | 4ºC |
| Specific gravity | 1 |

## Maximum Density

The maximum density temperature of water is 4ºC.

Most materials expand as their temperature rises, and water expands when heated above this temperature.  It is unusual, however, in that it also expands when cooled below this temperature.

Pure water boils at 100ºC at standard atmospheric pressure, and changes from a liquid to a gaseous state, expanding some 1,600 times as it does so.  This gas is referred to as steam and has various applications in the plumbing industry.  For example, steam may be used in large heating systems, or as a sterilising medium in hospitals, or even used as a source of power to drive a steam turbine.

Pure water freezes at 0ºC and changes from a liquid to a solid state called ice, with an immediate expansion of one tenth.

Thus, if the water in a 100mm tube were to freeze, all expansions were lengthways, the column of ice formed would be 110mm, or one tenth of the original volume of water, projecting beyond the end of the tube.

The force of this expansion is considerable, exerting great pressure on internal surfaces of pipes, which frequently burst under the strain.  It is therefore very important that adequate precautions are taken to prevent damage to pipes by frost.

Water Density

## Water Expansion

Expansion of Water

## Specific Gravity

Pure water is the standard substance with which the weight and volume of all substances are compared.

Water is always shown with a specific gravity figure of 1.  Any material with a specific gravity figure higher than 1 will sink in water, and any material with a specific gravity figure of less than 1 will therefore float.

Specific gravity may be defined as the ratio of the weight of a given volume of any substance to the weight of the same volume of water at 4ºC. The table below gives specific gravity figures and other relevant details of materials used in the plumbing industry.

Specific Gravity Figures

| MATERIAL | CHEMICAL SYMBOL | SPECIFIC GRAVITY | MELTING POINT ºC |
| --- | --- | --- | --- |
| Water | H2O | 1.0 | 100 |
| Lead | Pb | 11.3 | 327 |
| Copper | Cu | 8.9 | 1,000 |
| Aluminium | Al | 2.7 | 660 |
| Cast Iron | Fe | 7.2 | 1,526 |
| Steel | Fe | 7.8 | 1,926 |

It is worth nothing that specific gravity figures not only make it possible to compare the weight of a substance with water; they also make it possible to compare the weights of substances with each other. For example the specific gravity of lead is 11.3 while that of aluminium is 2.7 therefore, lead is approximately four times heavier than aluminium.

### Specific Gravity of Materials

Specific Gravity of Materials

| Water | 1 |
| --- | --- |
| Lead* | 11.3 |
| Aluminium | 2.7 |
| Cork** | 0.15 |
| Polystyrene | 0.015 |

*Lead is approx. 4 times heavier than aluminium.

**Cork is 10 times heavier then polystyrene.

Each apprentice will pressure test sample pipe-work to 6 bar.

Unit Exercise/Procedure No. 2.1.8.A

# Self Assessment

Calculate the capacity of a Ø50mm pipe 6m in length.

Calculate the volume and capacity of a cylinder 600mm in diameter x 1.2m high.

Calculate the volume and capacity of a storage tank 1.25m long x .75m high x 600mm wide.

Explain what is meant by maximum density of water.

Identify each of the following fittings in the diagram below.

Identify fittings diagram

# Index

H

hydrogen	20

L

liquid	20

M

maximum density	21

mild steel pipe

assembly	14

cutting	15

identification	12

Mild steel pipe

identification	10

O

odourless	20

oxygen	20

P

pipe cutting

mild steel	18

S

specific gravity	24

T

thread cutting	19

transparent	20

# Text boxes

32mm Schedule 80

32mm Blue Band

Wall

Thickness

3.25mm

Wall

Thickness

4.05mm

Wall

Thickness

5.08mm

32mm Red Band