| Trade of Metal Fabrication |
| --- |
| Module 1: | Basic Fabrication |
| Unit 12: | Abrasive Grinding and Cutting |
|  | Phase 2 |

Table of Contents

List of Figures	4

List of Tables	5

Document Release History	6

Module 1 – Basic Fabrication	7

Unit 12 – Abrasive Grinding and Cutting	7

Learning Outcome:	7

Key Learning Points:	7

Training Resources:	7

Key Learning Points Code:	7

Angle Grinder	8

Changing Discs	10

Grinding	11

Cutting Action	11

Sharpening Cutting and Small Tools	11

Precautions when Grinding	12

The Wheel	12

Wheel Balance	12

The Work Rest	12

Wheel Speed	12

British Standard Marking System for Abrasive Wheels	13

Abrasive	14

Grain	14

Grade	14

Conversion Tables	16

Self Assessment	19

Questions on Background Notes – Module 1.Unit 12	19

Index	20

# List of Figures

Figure 1 - Angle Grinder 1	8

Figure 2 - Angle Grinder 2	9

Figure 3 - Angle Grinder 3	9

Figure 4 – Angle Grinder Accessories	9

# List of Tables

Table 1 - Technical Data Ag 125-S Abrasive Grinder	8

# Document Release History

| Date | Version | Comments |
| --- | --- | --- |
| 24/08/06 | First draft |  |
| 13/12/13 | SOLAS transfer |  |

# Module 1 – Basic Fabrication

## Unit 12 – Abrasive Grinding and Cutting

Duration – 2 Hours

### Learning Outcome:

By the end of this unit each apprentice will be able to:

Identify  various grades of grinding disc by specification

State the types of portable grinding machines

Describe an abrasive wheel cutting machine

Identify types of cutting and grinding discs used with angle grinder

Identify safety procedures

### Key Learning Points:

| Rk | Types and grades of grinding discs. |
| --- | --- |
| Rk | Specifications. |
| Rk Sk | Changing discs. |
| Rk H | Ratio of speeds between machine and discs. |
| Rk H | Portable grinders. (See “Portable Grinding Machines” section in Module 1 Unit 10). |
| Rk H | Cutting and grinding discs. |
| Rk H | Abrasive wheel cutting machines. (See “Abrasive Wheel Cutting-Off Machines” section in Module 1 Unit 10). |
| Rk H | Safety procedures – safety awareness. (See “Basic Safety Rules” section in Module 1 Unit 10). |
| P | Communication, safe work practice and attitude. |

### Training Resources:

Workshop – portable grinders. Hand tools, drills. Types of specifications. Sample wheel. Instructor lecture and demonstrations. Texts, notes and handouts.

### Key Learning Points Code:

M = Maths	           D= Drawing     RK = Related Knowledge Sc = Science

P = Personal Skills	Sk = Skill	   H = Hazards

# Angle Grinder

Uses:

Grinding and cutting steel and metal

| Power Input | 1020 V |
| --- | --- |
| Power output | 600 W |
| No-load speed | 11.000 r.p.m. |
| Cutting disc diameter | Max. 125 mm |
| Drive spindle thread | M14 |
| Cutting depth | Max. 35 mm |
| Weight | Approx. 1.8 kg |

Table 1 - Technical Data Ag 125-S Abrasive Grinder

Features:

Dust protection for longer carbon brushes life

A slimmer design that lies well in the hand

Permanent on/off switch

Low vibration side handle (optional)

Side handle can be mounted on the left or right

Additional cooling slots for perfect cooling

Figure 1 - Angle Grinder 1

Figure 2 - Angle Grinder 2

Figure 3 - Angle Grinder 3

Figure 4 – Angle Grinder Accessories

Kwik-lock nut

Flange

M14 clamping nut

B35 pin wrench
Tool for changing discs.

# Changing Discs

To mount a grinding/cutting disc on an angle–grinder:

- Select a disc – cutting, grinding, size etc.

- Make sure that they are no defects in the disc (visually examine for cracks).

- All mating parts should be clean and free from grease
- Disc/flange faces
- Spindle threads/flange threads (if threaded type)

- Assembly
(a) Flanges located in correct position
(b) Spindle nut/clamping nut seated properly over disc securing it in position
(c) Pressing in bottom to hold/lock disc whilst tightening spindle nut/clamping nut
(d) Use pin wrench/tool for changing discs

# Grinding

## Cutting Action

The grinding wheel is made up of small grains of abrasive material called grit. The grit is embedded in a softer substance called the bond. The grit size and the bond material will vary according to the type of work on which the wheel is to be used.

If we examine an abrasive wheel closely the grit can be seen held together by the bond.

As the work is applied to the wheel the grit cuts the metal in a manner similar to a cutting tool. As the grit becomes blunt, voids which are present in the bond release the grit, which exposes new grit to continue the cutting action.

## Sharpening Cutting and Small Tools

Hand tools such as cold chisels, centre punches and scribers are easily and quickly sharpened on the off hand grinding machine (shown opposite). Drills can, and are, frequently sharpened on the off hand grinder.

Large drills, however, cannot be sharpened accurately and must be ground on a special machine or by using a fixture attached to the off hand grinder.

Single point tools as used on the lathe or sharper will frequently require sharpening. This can be achieved by setting the tool rest to the required angle and applying the tool to the wheel of the off hand grinder as shown here.

# Precautions when Grinding

## The Wheel

Due to the nature of its construction the wheel can, if not carefully treated, crack or even shatter during use. To reduce the danger of flying particles causing injury, the wheel must be guarded with only the working area exposed. Examine the wheel frequently for cracks or other defects.

When grinding move the work from side to side to avoid cutting grooves in the wheel. Use the front of the wheel as much as possible. If the side of the wheel is used avoid using too much force.

## Wheel Balance

During use it is quite common for the wheel to wear unevenly so that it runs out of true. Excessive vibration when running usually indicates that the wheel is out of balance.

The wheel can be trued up by using an abrasive stick or a star wheel dresser as shown.

Dressing the wheel also opens up the grit if the wheel has become loaded (blocked with dirt, grease or other matter).

## The Work Rest

When using the off hand grinder the work rest must be as close to the wheel as possible. Failure to observe this rule may result in the work becoming jammed between the wheel and rest.

## Wheel Speed

Never exceed the manufacturer’s recommended wheel speed. This speed is clearly indicated on the label on the side of the wheel. Always mount the wheel correctly.

# British Standard Marking System for Abrasive Wheels

The British Standard Marking System denotes the composition an9 qualities of abrasive wheels.

All wheels are marked to show 5 qualities:

ABRASIVE

GRAIN

GRADE

STRUCTURE

BOND

A thorough understanding of this marking system will help one to always select the correct abrasive wheel for the particular job in hand.

## Abrasive

The symbols ‘A’ or ‘C’ denote the abrasive used;

‘A’ - Aluminium Oxide - is ideal for grinding high-tensile material like steel.

‘C’ - Silicon Carbide - is used to grind materials of low-tensile strength like masonry or cast iron.

## Grain

Aluminium Oxide and Silicon Carbide abrasive grains are screened into various sizes.

The larger grains are contained in wheels used for maximum stock removal, the smaller ones in wheels used for minimum stock removal and fine finishing.

Grain size is indicated by various numbers between 8 (coarse) and 600 (very fine).

## Grade

This indicates the strength of the wheel, or, more precisely, the strength with which the bonding materials hold the abrasive grains in the wheel.

Abrasive grains act like thousands of cutters removing stock by tearing into the workpiece.

After some time they become blunt and must fall away if the wheel is to function correctly.

As they fall away new sharp abrasive grains are exposed for use.

Generally speaking, the harder the material being ground the quicker the grains lose their edge.

So, for grinding hard materials a soft grade wheel is used and for grinding soft materials a hard grade wheel is used.

Using too hard a wheel on a hard workpiece generates too much heat. This glazes the wheel and ruins the workpiece.

Using too soft a wheel on a soft workpiece results in excessive wheel wear and wastage.

Grade selection is made from an alphabetical list from A to Z.

‘E’ e.g. denotes a soft grade wheel suitable for grinding very hard materials like tungsten carbide and stainless steel.

‘U’ e.g. denotes a hard grade wheel suitable for grinding soft materials like aluminium.

# Conversion Tables

Sometimes instead of in r.p.m., wheel speeds are shown in surface feet per minute (S.F.P.M.) – that is, the number of feet the circumference of the wheel would travel in one minute.

Surface Feet per Minute to Revolutions per Minute

For surface speeds greater than 10,000 S.F.P.M. take half the diameter and double the r.p.m. from the chart below.

Note: Vitrified bond must never exceed 6,500 S.F.P.M. Organic bond (resinoid, rubber or shellac) may exceed 6,500 S.F.P.M.

| Grinding Wheel Speeds High Speed Table |
| --- |
| Diameter of Wheels | 7,000 S.F.P.M. | 8,000 S.F.P.M. | 9,000 S.F.P.M. | 10,000 S.F.P.M. |
| Ins. | m/m | r.p.m. | r.p.m. | r.p.m. | r.p.m. |
| 1 | 25.4 | 20,738 | 30,558 | 34,377 | 38,197 |
| 2 | 50.8 | 13,369 | 13,279 | 17,159 | 19,098 |
| 3 | 70.2 | 8,913 | 10,188 | 11,459 | 12,732 |
| 4 | 101.6 | 6,684 | 7,639 | 8,304 | 9,549 |
| 5 | 127 | 5,347 | 6,111 | 6,573 | 7,639 |
| 6 | 152 | 4,466 | 5,093 | 5,729 | 6,366 |
| 7 | 178 | 3,820 | 4,363 | 4,911 | 5,457 |
| 8 | 203 | 3,342 | 3,820 | 4,297 | 4,775 |
| 10 | 254 | 2,674 | 3,056 | 3,439 | 3,820 |
| 12 | 305 | 2,223 | 2,546 | 2,563 | 3,183 |
| 14 | 356 | 1,910 | 2,183 | 2,455 | 2,728 |
| 16 | 406 | 1,671 | 1,910 | 2,148 | 2,357 |
| 18 | 457 | 1,485 | 1,698 | 1,910 | 2,122 |
| 20 | 503 | 1,337 | 1,528 | 1,719 | 1,810 |
| 22 | 559 | 1,215 | 1,359 | 1,563 | 1,756 |
| 24 | 609 | 1,114 | 1,273 | 1,432 | 1,591 |
| 26 | 660 | 1,028 | 1,175 | 1,322 | 1,469 |
| 28 | 711 | 966 | 1,091 | 1,226 | 1,364 |
| 30 | 762 | 891 | 1,018 | 1,140 | 1,273 |
| 32 | 813 | 835 | 955 | 1,074 | 1,194 |
| 34 | 863 | 786 | 899 | 1,101 | 1,123 |
| 36 | 914 | 743 | 840 | 833 | 1,061 |

| Grinding Wheel Speeds Low Speed Table |
| --- |
| Diameter of Wheels | 4,000 S.F.P.M. | 5,000 S.F.P.M. | 6,000 S.F.P.M. | 6,500 S.F.P.M. |
| Ins. | m/m | r.p.m. | r.p.m. | r.p.m. | r.p.m. |
| 1 | 25.4 | 15,279 | 10,098 | 22,918 | 24,828 |
| 2 | 50.8 | 7,639 | 9,549 | 11,459 | 12,414 |
| 3 | 70.2 | 5,093 | 6,368 | 7,639 | 8,276 |
| 4 | 101.6 | 3,820 | 4,775 | 5,729 | 6,207 |
| 5 | 127 | 3,066 | 3,820 | 4,584 | 4,906 |
| 6 | 152 | 2,548 | 3,183 | 3,820 | 4,138 |
| 7 | 178 | 2,183 | 2,723 | 3,274 | 3,547 |
| 8 | 203 | 1,910 | 2,387 | 2,805 | 3,103 |
| 10 | 254 | 1,528 | 1,910 | 2,292 | 2,483 |
| 12 | 305 | 1,273 | 1,591 | 1,910 | 2,069 |
| 14 | 356 | 1,091 | 1,304 | 1,637 | 1,773 |
| 16 | 406 | 956 | 1,194 | 1,432 | 1,532 |
| 18 | 457 | 849 | 1,001 | 1,273 | 1,379 |
| 20 | 503 | 764 | 955 | 1,146 | 1,241 |
| 22 | 559 | 694 | 868 | 1,042 | 1,128 |
| 24 | 609 | 637 | 796 | 955 | 1,034 |
| 26 | 660 | 588 | 734 | 881 | 953 |
| 28 | 711 | 540 | 682 | 818 | 887 |
| 30 | 762 | 500 | 637 | 764 | 828 |
| 32 | 813 | 477 | 597 | 716 | 776 |
| 34 | 863 | 449 | 562 | 674 | 730 |
| 36 | 914 | 424 | 530 | 637 | 690 |

# Self Assessment

# Questions on Background Notes – Module 1.Unit 12

No Suggested Questions and Answers.

# Index

A

Angle Grinder, 8

B

British Standard Marking System for Abrasive Wheels, 13

Abrasive, 14

Grade, 14

Grain, 14

C

Changing Discs, 10

Conversion Tables, 16

G

Grinding, 11

Cutting Action, 11

Sharpening Cutting and Small Tools, 11

P

Precautions when Grinding, 12

The Wheel, 12

The Work Rest, 12

Wheel Balance, 12

Wheel Speed, 12

# Text boxes

A

C

For High-Tensile Materials e.g. Steel

For Low-Tensile Materials e.g. Cast Iron

Large Grain

Small Grain

For Maximum Stock Removal & Coarse Finish

For Minimum Stock Removal & Fine Finish

ABRASIVE

GRAIN

Soft Grade

Hard Grade

For Hard Materials       e.g. Stainless Steel

For Soft Materials      e.g. Aluminium

GRADE

Dense

Open

For Hard & Brittle Materials e.g. Hardened Steel

For Soft Materials      e.g. Soft Steel

STRUCTURE

Vitrified

Resinoid

Used only on Fixed Machines

Used only on Portable Machines

BOND