| Trade of Metal Fabrication |
| --- |
| Module 2: | Thermal Processes |
| Unit 2: | Oxy/Fuel Cutting Machine |
|  | Phase 2 |

Table of Contents

List of Figures	4

List of Tables	5

Document Release History	6

Module 2 – Thermal Processes	7

Unit 2 – Oxy/Fuel Cutting Machine	7

Learning Outcome:	7

Key Learning Points:	7

Training Resources:	7

Key Learning Points Code:	7

Typical Light-Duty Oxygen Cutting Machine	8

Profile Cutting Machine Tracing Heads	9

Allowances for Flame Cutting	11

Self Assessment	12

Questions on Background Notes – Module 2.Unit 2	12

Index	13

# List of Figures

Figure 1 - Typical Light-Duty Oxygen Cutting Machine	8

Figure 2 - Profile Cutting Machine Tracing Heads	9

# List of Tables

Table 1 - Cutting Data for Profile Cutting Machines	10

# Document Release History

| Date | Version | Comments |
| --- | --- | --- |
| 18/10/06 | First draft |  |
| 13/12/13 | SOLAS transfer |  |

# Module 2 – Thermal Processes

## Unit 2 – Oxy/Fuel Cutting Machine

Duration – 8 Hours

### Learning Outcome:

By the end of this unit each apprentice will be able to:

Set up Oxy/Fuel cutting machine

Operate Oxy/Fuel cutting machine safely and use cutting track-radius bar

### Key Learning Points:

| Sk Rk | Assembly and maintenance of equipment. (See “Equipment Assembly” section in Module 2 Unit 1). |
| --- | --- |
| Rk | Cutting techniques, cutting data, gas pressures, cutting speeds. (See “Cutting Techniques” section in Module 2 Unit 1). |
| Rk | Identification of various types of oxy/fuel cutting machines and their uses. |
| Sk | Cutting from templates. |
| H Rk | Hazard identification, safety standards and precautions. |
| M | Calculation for straight, regular and irregular cuts e.g. kerf width. |
| P | Communication, safety awareness and attitude. |

### Training Resources:

Fabrication workshop facilities

Oxy/Fuel cutting equipment – pug/quickie cutting machine & tracks

Instructor demonstrations and lectures

Handouts

Safety clothing and equipment

### Key Learning Points Code:

M = Maths	           D= Drawing     RK = Related Knowledge Sc = Science

P = Personal Skills	Sk = Skill	   H = Hazards

# Typical Light-Duty Oxygen Cutting Machine

Figure 1 - Typical Light-Duty Oxygen Cutting Machine

(Also known as profile cutter)

Key:

- Cutter (optional)

- Cutter

- Cutter mounting block

- Cutter mounting tube

- Trimming valve (heating oxygen)

- Trimming valve (fuel gas)

- Trimming valve (cutting oxygen)

- Web plates

- Grip knob

- Cutter mounting bar

- Cross carriage unit

- ON/OFF cock (cutting oxygen)

- Tracing table

- Drive unit

- Traversing carriage rails

- Rail connecting fitting

- Cross carriage rails

- Following head

- Mounting frame

- Cutter head mounting block

- Cutter head

- Work rests (optional)

# Profile Cutting Machine Tracing Heads

Figure 2 - Profile Cutting Machine Tracing Heads

Table 1 - Cutting Data for Profile Cutting Machines

To obtain the best results for accurate cutting, templates should conform to the following basic requirements.

- Minimum thickness 3 mm.

- Edges must be square. Plywood or hardwood templates should have their edges prepared with a coarse sandpaper finish, and metal template edges should have a good file finish but not too smooth, in order to provide sufficient frictional grip for the knurled steel rollers.

- When the inside corner of the component to be cut is radiused, the corner radius on the template must be greater than that of the roller.

- Correct allowances must be made in respect of the width of the KERF and the diameter of the tracing roller.

# Allowances for Flame Cutting

These will vary according to the width of the kerf, the diameter of the racing roller and whether an internal or external template is used.

The kerf

This is a term used to define the width of the metal consumed in the cutting process. It may vary between 1½ and 2 times the diameter of the cutting oxygen orifice of the cutting nozzle used; for example, a 1.6 mm diameter nozzle will produce a kerf of between 2.4 mm and 3.2 mm in width.

Allowances (to compensate for the kerf and the diameter of tracing roller) must be made on the size of the template and these will differ PLUS or MINUS depending whether an internal or external template is used.

For future use it is advisable to mark templates with the following information:

Nozzle type and size.

Fuel gas used.

Tracing roller diameter.

Thickness of plate cut.

Speed of cut.

Part number (if applicable) of component.

When using a WHEEL TRACING HEAD, allowances must be made on the drawing dimensions for the kerf width. As a general guide, allow the diameter of the cutting nozzle orifice per side, plus or minus for external and internal cuts respectively.

# Self Assessment

# Questions on Background Notes – Module 2.Unit 2

No Suggested Questions and Answers.

# Index

A

Allowances for Flame Cutting, 11

P

Profile Cutting Machine Tracing Heads, 9

T

Typical Light-Duty Oxygen Cutting Machine, 8