| Trade of Metal Fabrication |
| --- |
| Module 3: | Plate Fabrication |
| Unit 8: | Square to Square Hopper |
|  | Phase 2 |

Table of Contents

List of Figures	4

List of Tables	4

Document Release History	5

Module 3 – Plate Fabrication	6

Unit 8 – Square to Square Hopper	6

Learning Outcome:	6

Key Learning Points:	6

Training Resources:	7

Key Learning Points Code:	7

Twist Drill Cutting Speeds and Feeds	8

Self Assessment	12

Index	13

# List of Figures

Figure 1 - Types of Twist Drill	8

Figure 2 - Twist Drill Cutting Angles	9

Figure 3 - Helix Angles	10

# List of Tables

Table 1 - Metric Size Drills (mm)	9

Table 2 - Cutting Speeds for HSS Twist Drills	11

Table 3 - Feeds for HSS Twist Drills	11

# Document Release History

| Date | Version | Comments |
| --- | --- | --- |
| 20/12/06 | First draft |  |
| 13/12/13 | SOLAS transfer |  |

# Module 3 – Plate Fabrication

## Unit 8 – Square to Square Hopper

Duration – 10 Hours

### Learning Outcome:

By the end of this unit each apprentice will be able to:

Read and interpret drawing

Mark out material, flame cut, drill, assemble and weld a square to square hopper to standard of ± 2mm

### Key Learning Points:

| Sk Rk | Handling of materials – safety. (Also see Module 3 Unit 7). |
| --- | --- |
| Rk | Economic use of material. (Also see Module 3 Unit 7). |
| Rk | Application of square to square hoppers in industry. (Instructor explains this in classroom). |
| Sk Rk | Methods of development, radial line, triangulation. (Instructor explains this in classroom). |
| Rk | Bending – bend allowance inside and outside dimensions. (Also see Module 3 Unit 1). |
| Rk | True lengths – Pythagoras Theorem. (Instructor explains this in classroom). |
| Sk | Flame cutting. |
| Rk Sk | Use of jigs – assembly. |
| Sk | Manual arc welding. |
| Rk | Drilling – speeds and feed rate, types of drill bits. |
| M | Indices – rules of manipulation of indexed terms expression in standard form. (Instructor explains this in classroom). |
| P | Presentation and standard of work. |

### Training Resources:

Fabrication workshop

Shears

Oxy/fuel cutting equipment

M.M.A.

Plant

Equipment and consumables

Apprentice tool kit

Pillar drill

Drill bits

5mm steel plate

50 x 6mm flat bar

Safety clothing and equipment

### Key Learning Points Code:

M = Maths	           D= Drawing     RK = Related Knowledge Sc = Science

P = Personal Skills	Sk = Skill	   H = Hazards

# Twist Drill Cutting Speeds and Feeds

Figure 1 - Types of Twist Drill

For a drill to give satisfactory performance it must operate at the correct speed and correct rate of feed. For optimum results it is essential that:

- The work is rigidly clamped.

- The machine is in good condition.

- A coolant is used if required.

- The drill is correctly selected and ground to suit the material being cut.

A craftsman should be capable of grinding a twist drill by hand; however, one can never equal the twist drill point-grinding machine for consistent results. Whenever possible, the point should be ground on such a machine and checked on a point angle gauge.

Table 1 - Metric Size Drills (mm)

Figure 2 - Twist Drill Cutting Angles

Figure 3 - Helix Angles

Table 2 gives a range of cutting speeds suitable for jobbing work. The rates of feed and cutting speeds for twist drills are lower than for most other machining operations. This is because:

- The drill is relatively weak compared with other cutting tools – the cutting forces are only resisted by the slender web.

- In deep holes it is relatively difficult for the drill to eject the chips.

- It is difficult to keep the point and cutting edge cool when they are enclosed in a hole.

Table 2 - Cutting Speeds for HSS Twist Drills

Table 3 - Feeds for HSS Twist Drills

# Self Assessment

Questions on Background Notes – Module 3.Unit 8

No Suggested Questions and Answers.

# Index

T

Twist Drill Cutting Speeds and Feeds, 8