| Trade of Sheet Metalwork |
| --- |
| Module 3: | Thermal Processes |
| Unit 16: | Frame Work |
|  | Phase 2 |

Table of Contents

List of Figures	4

List of Tables	5

Document Release History	6

Module 3 – Thermal Processes	7

Unit 16 – Frame Work	7

Learning Outcome:	7

Key Learning Points:	7

Training Resources:	7

Key Learning Points Code:	7

Introduction	10

Hazard Statement	11

Hydraulic Power Saw	12

Safe Work Practices	12

Self Assessment	13

Answers to Questions 1-2. Module 3.Unit 16	14

Index	15

# List of Figures

Figure 1 – Frame Work 1	8

Figure 2 - Frame Work 2	9

Figure 3 - Hazard Statement	11

# List of Tables

# Document Release History

| Date | Version | Comments |
| --- | --- | --- |
| 13/10/06 | First draft |  |
| 07/04/14 | 2.0 | SOLAS transfer |

# Module 3 – Thermal Processes

## Unit 16 – Frame Work

Duration – 16 Hours

### Learning Outcome:

By the end of this unit each apprentice will be able to:

Tack and continuous weld work pieces A, B and C.

Clean, sand down and polish welds using disc sander, portable belt sander. (“dynafile”) with “Flexi-Shaft” machine.

### Key Learning Points:

| Sk | Deburring. |
| --- | --- |
| Sk | Positioning and tack welding. |
| Sk | No filler rod required for fillet weld – filler rod required elsewhere. |
| Sk | Joint restraint/jogs. |
| Sk | Care of tungsten tips. |
| Sk | Weld finishing. |
| Sk | Polishing and blending. |
| Rk Sk | Machinery – cut off Saw/band Saw. |

### Training Resources:

TIG welding plant

Toolkit

Disc sander and flexi-shaft

Safety clothing and equipment, reference library

32 x 32 x 1.2 stainless steel box section

1.2 mm stainless steel

Welding booths and fume extraction system

Machine accessories

Polishing materials

50 x 25 x 1.2 stainless steel box section

### Key Learning Points Code:

M = Maths	           D= Drawing     RK = Related Knowledge Sc = Science

P = Personal Skills	Sk = Skill	   H = Hazards

Figure 1 – Frame Work 1

Figure 2 - Frame Work 2

# Introduction

It is important before using any machinery to be aware of the dangers.

Read the safety manual provided with each piece of equipment and also the hazard warning statement (included).

# Hazard Statement

Figure 3 - Hazard Statement

# Hydraulic Power Saw

## Safe Work Practices

OBJECTIVE:

To cut round bars to length in a safe manner using Hydraulic Power Saw.

PERSONAL PROTECTIVE EQUIPMENT:

Safety boots, overalls, gloves (as required).

PROCEDURE:

- Inspect equipment to ensure there are no obvious defects.

- Lift cutting blade housing by handle to sufficient clearance for metal.

- Take out round bar from stack and place it in the clamp with the end supported by a stand.

- Measure the distance to be cut and drop down blade to near the point of cut.

- Make fine adjustment. Tighten clamp and adjust guard to width of material plus sufficient clearance.

- Switch on isolator switch with key.

- Press start button and weight using knob to control hydraulic pressure (as per instructions).

- When cut is finished machine cuts off automatically when pre-adjusted limit switch breaks connection.

- Switch off isolator using key.

SAFETY ISSUES:

- Always wear the prescribed personal protection.

- Exercise caution. Some bars are very heavy. Sometimes help will be required.

- Keep clear of blade whilst in motion.

- Ensure bar is properly supported at ends.

# Self Assessment

Questions on Background Notes – Module 3.Unit 16

1.     Is injury from band saw rated high or low?

2.    What is the greatest risk to the body from this machine?

# Answers to Questions 1-2. Module 3.Unit 16

1.

Risk injury from the band saw is rated high.

2.

Risk of eye damage from flying particles. It is also important to realise the damage to fingers and limbs as it is a powerful machine capable of cutting through steel.

# Index

H

Hazard Statement, 11

Hydraulic Power Saw, 12

Safe Work Practices, 12

I

Introduction, 10

S

Self Assessment, 14