| Trade of Sheet Metalwork |
| --- |
| Module 3: | Thermal Processes |
| Unit 5: | Oxy-acetylene Welding “T” Fillet |
|  | Phase 2 |

Table of Contents

List of Figures	4

List of Tables	5

Document Release History	6

Module 3 – Thermal Processes	7

Unit 5 – Oxy-acetylene Welding “T” Fillet	7

Learning Outcome:	7

Key Learning Points:	7

Training Resources:	7

Key Learning Points Code:	7

The Welding Flame	9

Self Assessment	10

Answers to Questions 1. Module 3.Unit 5	11

Index	12

# List of Figures

Figure 1 - Oxy-Acetylene Welding - T Fillet Joint	8

Figure 2 - Neutral Flame	9

Figure 3 - Carburising Flame	9

Figure 4 - Oxidising Flame	9

# List of Tables

# Document Release History

| Date | Version | Comments |
| --- | --- | --- |
| 14/09/06 | First draft |  |
| 08/04/14 | 2.0 | SOLAS transfer |

# Module 3 – Thermal Processes

## Unit 5 – Oxy-acetylene Welding “T” Fillet

Duration – 14 Hours

### Learning Outcome:

By the end of this unit each apprentice will be able to:

Read and interpret drawing and weld symbol

Select suitable nozzle, set gas pressures, light torch and adjust flame to the neutral position

Arrange and tack weld the plates to form a “T” fillet joint

Complete the fillet weld in mild steel sheet 1.2 mm and 1.5 mm mild steel sheet

### Key Learning Points:

| P | Weld symbol. |
| --- | --- |
| P | Nozzle size, gas pressures. |
| Rk P | Flame adjustment. |
| Sc P | Tacking procedure – joint set-up. |
| P P | Welding technique – rod/torch angle, torch manipulation. |
| Sk P | Safety precautions – hazards. |
| H P | Weld profile – leg length, throat thickness. |

### Training Resources:

Oxy-acetylene welding equipment

Safety clothing and equipment

Material 1.2 mm and 1.5 mm mild steel sheet

Toolkit

Drawing and hand-outs

Figure 1

### Key Learning Points Code:

M = Maths	           D= Drawing     RK = Related Knowledge Sc = Science

P = Personal Skills	Sk = Skill	   H = Hazards

Figure 1 - Oxy-Acetylene Welding - T Fillet Joint

# The Welding Flame

Neutral Flame 
(equal quantities of oxygen and acetylene).

Figure 2 - Neutral Flame

Carburising Flame 
(excess acetylene) 
Note: feather at cone.

Figure 3 - Carburising Flame

Oxidising Flame 
(excess oxygen).

Figure 4 - Oxidising Flame

# Self Assessment

Questions on Background Notes – Module 3.Unit 5

1.     Name and describe the three types of flame used in gas welding.

# Answers to Questions 1. Module 3.Unit 5

1.

Neutral Flame: Equal quantities of 02 and acetylene. Carbonising Flame: An excess of acetylene. Oxidising Flame: An excess of 02.

# Index

T

The Welding Flame, 9