| Trade of Sheet Metalwork |
| --- |
| Module 4: | General Sheet Metalwork |
| Unit 9: | Right Cone Cut by a Curve |
|  | Phase 2 |

Table of Contents

List of Figures	4

List of Tables	5

Document Release History	6

Module 4 – General Sheet Metalwork	7

Unit 9 – Right Cone Cut by a Curve	7

Learning Outcome:	7

Key Learning Points:	7

Training Resources:	7

Key Learning Points Code:	7

Cone Cut by a Curve	9

Self Assessment	10

Answers to Questions.  Module 4.Unit 9	11

Index	12

# List of Figures

Figure 1 - Cone Cut by Curve	8

# List of Tables

# Document Release History

| Date | Version | Comments |
| --- | --- | --- |
| 17/11/06 | First draft |  |
| 09/04/14 | 2.0 | SOLAS transfer |

# Module 4 – General Sheet Metalwork

## Unit 9 – Right Cone Cut by a Curve

Duration – 10.5 Hours

### Learning Outcome:

By the end of this unit each apprentice will be able to:

Construct and fabricate a right cone intersecting a cylindrical main duct using  parallel and radial line method of development

Assemble a cylindrical spigot using a paned-down joint

Plan and organise the production sequence

Form individual parts

### Key Learning Points:

| D | Drawing and development of right cone cut by a curve. |
| --- | --- |
| Rk | Accuracy required for curved developments. |
| Sk | Fit up of curved surface to cylindrical pipe. |
| P | Work unassisted. |

### Training Resources:

Toolkit

Work sample

Spot welding machine (pedestal or hand type)

Conical bench stakes

Job card

Job notepad

Safety equipment and protective clothing

0.6mm galvanised mild steel

### Key Learning Points Code:

M = Maths	           D= Drawing     RK = Related Knowledge Sc = Science

P = Personal Skills	Sk = Skill	   H = Hazards

Figure 1 - Cone Cut by Curve

# Cone Cut by a Curve

If pipe B is marked out by parallel line development, the work shop method to obtain the hole of penetration may be used to check out your drawing accuracy.

- Using the measurements given draw these two views.

- Use the radial line as shown earlier.

- Finished pattern should look like pattern A.

# Self Assessment

Questions on Background Notes – Module 4.Unit 9

No suggested Questions and Answers.

# Answers to Questions.  Module 4.Unit 9

No suggested Questions & Answers.

Index

C

Cone Cut by a Curve, 9