| Trade of Sheet Metalwork |
| --- |
| Module 5: | Ductwork |
| Unit 2: | 90° Square Bend with 'S' & 'C' Cleats |
|  | Phase 2 |

Table of Contents

List of Figures	4

List of Tables	5

Document Release History	6

Module 5 – Ductwork	7

Unit 2 – 90° Square Bend with 'S' & 'C' Cleats	7

Learning Outcome:	7

Key Learning Points:	7

Training Resources:	7

Key Learning Points Code:	7

Components of an Extraction Ventilation System	11

Self Assessment	12

Answers to Questions 1-3. Module 5.Unit 2	13

Index	15

# List of Figures

Figure 1 - 90° Square Bend	8

# List of Tables

# Document Release History

| Date | Version | Comments |
| --- | --- | --- |
| 11/01/07 | First draft |  |
| 09/04/14 | 2.0 | SOLAS transfer |

# Module 5 – Ductwork

## Unit 2 – 90° Square Bend with 'S' & 'C' Cleats

Duration – 3.5 Hours

### Learning Outcome:

By the end of this unit each apprentice will be able to:

Sketch 90° square bend(front elevation, end view and pictorial)

Mark out and fabricate 90° square bend with square heel and throat for use with ‘S’ and ‘C’ cleats

Job planning

### Key Learning Points:

| Rk | Parts of bend – throat, heel and cheeks. |
| --- | --- |
| Rk | Cross joints – ‘S’ and ‘C’ cleats. |
| Rk | Marking out, notching procedure – cheeks first. |
| Rk Sk | Fabrication and assembly techniques. |
| P | Job planning/sequence of operations. |
| M | Measure check/wrapper size. Measure area/weight of metal in square. |
| Sc | Pressure/ductwork design. |

### Training Resources:

Toolkit

Tools and machinery/equipment

Workshop drawing

Live  example

0.6mm galvanised mild steel

Metal manufacturer’s weight tables

Reference library

Safety equipment and protective clothing

Calculator
a. DW/143
b. DW/144
c. DW/TM2
d. TR-17
e. DW-171
f. BS5970:2001

### Key Learning Points Code:

M = Maths	           D= Drawing     RK = Related Knowledge Sc = Science

P = Personal Skills	Sk = Skill	   H = Hazards

Figure 1 - 90° Square Bend

This bend is made up of 4 parts, 2 cheeks – one of which is visible from the plan. They are referred to as the left and right cheeks when looked at in the end view. The throat has the smaller dimensions, i.e. 150 x 150 and the heel is the back of the bend measuring 300 x 300 on first observations. Depending on the type of joint we may add or subtract from the above measurements.

As we are using S and C cleats the sizes are indeed 150 x 150mm and 300 x 300mm. We bend 12.5mm back as seen in the drawing to make the C cleat.

To make up the cheeks cut metal blanks 310 x 310mm. 10mm is added for the Pittsburgh lock on the heel. There is no need to add on 10mm for the Pittsburgh lock at the throat. The cheeks look like so. We notch the shaded areas which are part of the lockform joint and slit the 10mm throat were shown. We also remove 140 x 140 from the throat section.

The throat and heel wrappers are notched at both ends to suit a C cleat. We simply cut out 35 x 25mm for the lockform and bend on a line 12.5mm in from each end. To obtain area/weight of metal we multiply L x W and subtract all the notched out areas to get a more accurate answer.

This is the easiest 90° bend to make. While quick and economical the airflow is not as efficient as our next bend - a radius bend. We may put in turning vanes to help improve air flow.

The throat is notched similar only the middle changing slightly to a deeper notch as bending on the middle line is o/s instead of i/s.

We notch into the 35mm line and come out 6mm each side of the bend line approximately. This prevents a bulging of the metal in the throat section and allows for easier bending.

# Components of an Extraction Ventilation System

- Fan

- Ductwork itself

- Fittings, i.e. bends, offsets, reducers etc.

- Grills

- Louvers

- V.C.D.

- Fire dampers

- Access doors

- Roof curb

- Flashing

- Weather cap/apron

- Roof cowl

# Self Assessment

Questions on Background Notes – Module 5.Unit 2

1.     What is the area of the two cheeks?

2.      What % of this area is scrap? You may disregard the triangular portions if you

so wish.

3.      Sketch an S and C cleat giving it nominal dimensions.

# Answers to Questions 1-3. Module 5.Unit 2

1.

The amount of metal used is simply: L x B i.e. 300 x 300mm = 90,000mm²

2.

The major part of the scrap is the: Throat area 150 x 150mm = 22,500mm² This is ¼ of 90,000 the total area and so 25% being the same as ¼ Our answer is: 90,000 = 100% = 1% 900 = 1% = 25%

3.

Figure 1: S Cleat Figure 2: C Cleat

# Index

C

Components of an Extraction Ventilation System, 11

S

Self Assessment, 12