TRADE OF

VEHICLE BODY REPAIR

PHASE 2

Module 5

UNIT: 2

Spray – Painting Equipment

Produced by

In cooperation with subject matter expert:

Maurice Stack

Some material courtesy of CDX Global and
FENC – Further Education National Consortium.

© SOLAS 2014

Table of Contents

Introduction	7

Unit Objective	8

Spray-Painting Equipment	8

1.0 Installation - Spray gun	10

1.1 Operation	10

1.2 Preventative Maintenance	11

2.0 Air Atomizing Spray Gun	12

2.1 Air Brush Kits, Spares and Accessories	16

3.0 Maintenance on a Spray Gun	18

3.1  Spray Gun Dismantling and Reassembling Component Parts and Seals	18

3.2  Devilbiss PRi.	20

3.3  GTi, GTiW Gravity Feed	22

3.4  The GTi	24

3.5  DeVilbiss SRi/ SRi W - Spot Repair Gun	25

3.6  Pro Range of Gravity Spray Guns for Primer, Basecoat and Clearcoat	30

3.7  GTi Pro	32

3.8  In-Line Air Adjusting Value	32

3.9  Spray Gun Cleaning Kit	33

3.10 Cup Filters	34

3.11 Viscosity Cups	34

3.12 Duster Blow Guns	35

3.13 Spray Gun First Aid Kits	35

3.14 Mixing Cups	36

3.15 Spray Gun Oil	36

3.16 SATAjet® 2000 HVLP Digital	37

3.17 SATAjet 2000 HVLP Digital 2	38

4.0 Inspect and Carry out Maintenance on Air Hoses	40

4.1 Air Hose Construction	40

4.2 Hose Construction	41

5.0 Calculate the Pressure Drop in an Airline	42

5.1 Airline Pressure Drop	42

6.0 Inspect and Carry Out Routine Maintenance on an Air Compressor	43

7.0 Type of Air Compressors	46

8.0 Pressure and Volume	49

9.0 Carry Out Routine Maintenance on Air Transformers	50

9.1 Routine Compressor Maintenance	51

10.0 Personal Safety	53

11.0 Compressed Air Pipeline Layout for Spray Room	54

12.0 Spray booth operating controls and housekeeping	55

12.1 Use and clean a spray booth	55

13.0 Choose and Use Different Paint Drying Equipment	56

13.1 Waterborne Paint Air Blowing Equipment	56

13.2 Infrared Drying Equipment	61

13.3 UV Drying	62

14.0 Terminology & Definitions	63

15.0 Compressed Air Pipeline Layout for Work Shop	67

Summary	68

Self Assessment	69

Suggested Exercise

Training Resources

Table of Figures

Figure 1: GFG Spray Gun	9

Figure 2: Suction Feed Gun with Attached Cup	12

Figure 3: Pressure Feed Gun with Remote 2 gal. Cup	12

Figure 4: Pressure Feed Air Cap	13

Figure 5: Bleeder Type Gun	13

Figure 6: Non-Bleeder Type Gun	14

Figure 7: External Mix Gun	14

Figure 8: Internal Mix Gun	14

Figure 9: Airbrush	15

Figure 10: Airbrush Kit	15

Figure 11: Principle Parts of a Spray Gun	17

Figure 12: Main Items and Assemblies for JGA	18

Figure 13: Devilbiss	21

Figure 14: The GTi	24

Figure 15:  DeVilbiss SRi	28

Figure 16: GTi Pro Spray Gun	31

Figure 17: SATAjet® 2000 HVLP Digital	37

Figure 18: SATAjet® 2000 HVLP Digital 2	38

Figure 19: Hose Construction	41

Figure 20: Piston Type Compressor	43

Figure 21: Piston Compressor	44

Figure 22: Two-Stage Compressor	45

Figure 23: Piston Type Compressor	46

Figure 24: Rotary Vane Compressor	47

Figure 25: Screw Type Compressor	47

Figure 26: Air Transformer	50

Figure 27: Pipeline Layout for Spray Room	54

Figure 28: Installation of Stand	58

Figure 29: Spraybooth	60

Figure 30: Infra Red Short Wave	62

Figure 31: Compressed Air Pipeline Layout	67

Introduction

Use and maintenance of refinishing equipment, spray guns, cups, compressors, regulators, hoses, spray booths, respirators is of the utmost importance, for to create a perfect finish definitely requires a solid knowledge of surface preparation.

But even an extensive knowledge of surface preparation techniques and paint chemistry is not enough to assure a professional finish. It must still be applied by a spray gun and all of the variables of its use must be controlled. The equipment necessary to apply the finish; the spray gun, cup, regulator, hoses, compressor, etc. must all be matched to the job and to each other. The equipment must be used and maintained properly, with an appreciation of how it works and why is works the way it does.

The moment of truth for any finish is when the trigger is pulled on the gun.

Unit Objective:

Spray-Painting Equipment

By the end of this unit each apprentice will be able to:

- Carry out maintenance on a spray gun

- Inspect and carry out maintenance on air hoses

- Calculate the pressure drop in an airline

- Carry out routine maintenance on air transformers

- Inspect and carry out routine maintenance on an air compressor

- Use and clean a spray booth

- Choose and use different paint drying equipment

Key Learning Points:

- Spray gun schematic drawings

- Spray gun component

- Parts and seals

- Spray gun dismantling and reassembling

- Air hose construction

- Airline pressure drop

- Types of air compressor parts

- Routine compressor maintenance

- Dangers and misuse of compressed air

- Spray booth operating controls and housekeeping

- Infrared drying equipment

- Waterborne paint air-blowing equipment

Figure 1: GFG Spray Gun

| Main Item and Assemblies for GFG |
| --- |
| Ref | Part No. | Description |
| 1 | MBC-368 | Air Cap Retaining Ring |
| 2 | JGD-402 | Air Baffle |
| 3 | 34411-122 | Fluid Needle Packing Nut |
| 4 | GFG-413 | Air Value Assembly |
| 5 | MBD-19 | Fluid Needle Spring |
| 6 | JGA-17 | Fluid Needle Body Bushing |
| 7 | JGS-16 | Fluid Needle Adjusting Screw |
| 8 | JGK-449 | Air Valve Assembly |
| 9 | JGS-431 | Air Valve Seat and Stem |
| 10 | 6000-12 | Control Valve Plug |
| 11 | PA-MB-51 P-MB-51 | Air Inlet Conn.¼" BSP or Air Inlet Conn.¼" NPS |
| 12 | JGS-108 | Trigger |
| 13 | KGP-401 | Cup Lid for KGP-503 (½ pint) |
| 13 | KGP-402 | Cup Lid for KGP-504 (1 pint) |
| 14 | KGP-503 | ½ Pint Cup Assembly |
| 14 | KGP-504 | 1 Pint Cup Assembly |
| 15 | 1718-30 | Washer |
| Replacement Spare Kits For GFG and JGA |
| Ref | Part No. | Description |
| A | JGD-14-R5 | Kit of Five Baffle Seals |
| B | JGA-4035-R2 | Kit of Five Needle Packings |
| C | SST-8434-K5 | Kit of Five Circlips |
| D | SSG-8069-K5 | Kit of Five ‘O’ Rings |
| E | JGS-72-K5 | Kit of Five Gaskets |
| F | MBD-12-K3 | Kit of Three Springs |
| G | A-42-K5 | Kit of Five Screws |
| H | JGS-35-K5 | Kit of Five Trigger Bearing Studs |
| I | 25746-007-K5 | Kit of Five Retaining Rings |
| J | KGP-2-K5 | Kit of Five Drip Check Cup Caps |
| K | KGP-5-K5 | Kit of Paint Strainers |

## 1.0 Installation - Spray gun

Important: To ensure that this equipment reached you in first class condition, protective coatings have been used. Flush the equipment through with a suitable solvent before use.

- Attach air hose to connector. Recommended hose 8mm bore. The hose must be conductive and electrical bond from the spray gun to earth should be checked with an ohmmeter. A resistance of less than 106Ω is recommended.

- Air supply should be filtered and regulated.

## 1.1 Operation

- Mix coating material to manufacturers instructions.

- Turn needle adjusting screw counter-clockwise until first thread shows.

- Turn pattern valve counter-clockwise to fully open.

- Adjust inlet air pressure to give 2 bar (29psi) as the gun inlet with the gun triggered.

- Test spray. If the finish is too dry, reduce airflow by reducing inlet pressure. If finish is too wet, reduce fluid flow by turning needle screw clockwise. If atomisation is too coarse, increase inlet air pressure. If too fine reduce inlet pressure.

- The pattern size can be reduced by adjusting valve.

- Hold gun perpendicular to surface being sprayed. Arcing or tilting may result in uneven coating.

- The recommended spray distance is 150-200 mm (6”-8”).

- Spray edges first. Overlap each stroke a minimum of 50%. Move gun at a constant speed.

- Always turn off air supply and relieve pressure when gun is not in use.

Air Flow Valve

If the airflow valve is fitted this can be used to reduce the inlet pressure through the gun. Screw the Adjusting Knob in to pressure.

1.2 Preventative Maintenance

- Turn off air supply and relive pressure in the airline, or if using QD system, disconnect from airline.

- Empty coating material into a suitable container and clean the gun and cup, preferably in a gun wash machine.

- IMPORTANT- the cup must not be cleaned or rubbed with a dry cloth or paper. It is possible to generate a static charge, by rubbing, which if discharged to an earthed object could create an incentive spark and cause solvent vapour to ignite. Only use a dampened cloth or antistatic wipes if additional cleaning is required in a hazardous area.

- Remove air cap and clean. If any of the holes in the cap are blocked with coating material use a toothpick to clean. Never use metal wire which could damage the cap and produce distorted spray pattern.

- Ensure the tip of the nozzle is clean and free from damage. Building up of dried paint can distort the spray pattern.

- Lubrication- stud-screw, needle and air valve should be oiled each day.

2.0 Air Atomizing Spray Gun

A spray gun is a tool which uses compressed air to atomize paint or other sprayable material and apply it to a surface. Air and the material enter the gun through separate passages and are mixed at the air cap in a controlled pattern.

Spray guns can be classified in various ways. One is by the location of the container. Figure 2 shows a gun with an attached cup. Figure 3 illustrates a gun using material from a container some distance away. The type of material feed system can also be a way of classifying guns, with the material either kept under pressure – a pressure feed gun (figure 3) or using the suction feed principle to deliver the material to the gun (figure 2).

Figure 2: Suction Feed Gun with Attached Cup

Figure 3: Pressure Feed Gun with Remote 2 gal. Cup

A spray gun design in which a stream of compressed air creates a vacuum at the air cap, providing a siphoning action. Atmospheric pressure on the material in the suction cup forces the material to the air cap of the gun. The vent holes in the cup lid must be open. This type gun is usually limited to quart-size or smaller containers. It is easily identified by the fluid tip extending slightly beyond the face of the air cap. Suction feed guns are suited to many colour changes and small amounts of material, such as in auto refinishing.

Pressure Feed Gun

In the design of the pressure feed gun the fluid tip is flush with the face of the air cap (figure 4) and no vacuum is created. The fluid is forced to the air cap by pressure kept on the material in the system: a separate cup, tank or pump. This system is normally used when large amounts of material are too heavy to be siphoned from a container, or when fast application is required. Production spraying in a manufacturing plant would be a typical use of a pressure feed system.

Figure 4: Pressure Feed Air Cap

Bleeder Type Gun

A bleeder type gun is designed without an air valve. Air passes through the gun at all times. It is usually used with small compressors of limited capacity and pressure which have no pressure-controlled device such as an unloader or pressure switch. In this type of gun (figure 5) the trigger only controls the flow of fluid.

Figure 5: Bleeder Type Gun

Non-Bleeder Type Gun

A non-bleeder type gun is equipped with an air valve to shut off the flow of air when the trigger is released: the trigger controls both air and fluid flow. It is used with compressors having some type of pressure control device.

Figure 6: Non-Bleeder Type Gun

External Mix Gun

This type, as shown in figure 7 mixes and atomizes air and fluid outside the air cap. It can be used for applying virtually all types of materials and is desirable for spraying fast drying paints such as lacquer. It is also used when a high quality finish is desired.

Figure 7: External Mix Gun

Internal Mix Gun

This gun type mixes air and material inside the air cap before expelling them, as shown in figure 8. it is usually used where low air pressures and air volumes are employed or where slow drying materials are being sprayed. A typical example would be spraying flat wall paint or outside house paint with a 1/4 or 1/3 HP compressor. Internal mix guns are rarely used for refinishing when very fast drying materials are being sprayed.

Figure 8: Internal Mix Gun

Airbrush

This is a very small, lightweight spray gun used for painting very fine detail such as stripes. It has a paint capacity of ½ to 1 ounce and the spray pattern is adjustable up to about the size of a 5c piece.

Figure 9: Airbrush

The Right Way to Finish™

Figure 10: Airbrush Kit

2.1 Air Brush Kits, Spares and Accessories

| Ref No. | Part No. | Description |
| --- | --- | --- |
| 1 | ABA-419-K ABA-603-K | High Flow Air Cap and Nozzle Kit Low Flow Air Cap and Nozzle Kit |
| 2 |  | Air Cap Guard |
| 3 | (Include in Ref.1.) | Air Cap |
| 4 |  | Nozzle |
| 5 |  | Nozzle ‘O’ Ring |
| 6 | A-105 | Needle Packings (Leather) |
| 7 | ABA-17 | Needle Packing Gland |
| 8 | ABA-404 | Control Lever |
| 9 | ABA-16 | Needle Spring |
| 10 | ABA-14 | Needle Collar |
| 11 | ABA-6 | Spring Box |
| 12 | ABA-27 | Clutch Piece |
| 13 | ABA-15 | Needle lock Nut |
| 14 | ABA-43-K2 ABA-25-K2 | High Flow Needle Kit (2 in Kit) Low Flow Needle Kit (2 in Kit) |
| 15 | ABA-425 | Handle |
| 16 | SPS-1741 | Air Valve Ball |
| 17 | ABA-55 | Air Valve Spring |
| 18 | NSA-13 | Air Valve Screw |

| Part No. | Description |
| --- | --- |
| ABA-406-K | Aerosol Valve |
| BMP-501 | Devair Aerosol |
| CT-845-K | 8ft Hose and Connections |
| ABA-439 | 1oz Bottle with Lid and Fluid Tube |
| ABA-25-K2/ABA-630-K | Fine Line Kit |

The Non-bleeder, external mix gravity or siphon feed gun is the most common gun used in the auto refinishing business. Small jobs such as panel repair, usually call for small amounts of paint and therefore a suction feed gun with a ¼cup would normally be used. For larger jobs requiring more material, a shop may use a pressure feed system with a separate larger material container.

Devilbiss Siphon Feed JGA Spray Gun

Devilbiss Gravity Feed GTI                                                                                                             Spray Gun

Part Identification Function

The principle components are illustrated in figure 11. Some guns are equipped with removable spray head unit containing the air cap, fluid tip and fluid needle.

Figure 11: Principle Parts of a Spray Gun

3.0 Maintenance on a Spray Gun

3.1 Spray Gun Dismantling and Reassembling Component Parts and Seals

Figure 12: Main Items and Assemblies for JGA

Main Items and Assemblies for JGA

| Ref | Part No. | Description |
| --- | --- | --- |
| 1 | MBC-368 | Air Cap Retaining Ring |
| 2 | JGD-402 | Air Baffle |
| 3 | 34411-122 | Fluid Needle Packing Nut |
| 4 | JGA-497 | Spreader Valve Assembly |
| 5 | MBD-19 | Fluid Needle Spring |
| 6 | JGA-17 | Fluid Needle Body Brushing |
| 7 | JGS-16 | Fluid Needle Adjusting Screw |
| 8 | JGK-449 | Air Valve Assembly |
| 9 | JGS-431 | Air Valve Seat and Stem |
| 10 | JGA-51 | Fluid Inlet Locknut |
| 11 | PA-MB-51 P-MB-51 | Air Inlet Conn.¼" BSP or Air Inlet Conn.¼" NPS |
| 12 | JGS-108 | Trigger |
| 13 | JGA-4005 | Air Flow Valve Assembly |
| 14 | PA-JGA-2-2 P-JGA-2-2 | Fluid Inlet Conn. ⅜"BSP or Fluid Inlet Conn. ⅜" NPS |

The PRi is a compliant gravity feed spray gun specifically developed for the application of modern primers, surfaces and sprayable fillers. The No.310 DevVilbiss Trans-Tech air cap provides excellent atomisation and lay down whilst complying with mandatory EPA legislation. The gun is easy to clean and maintain with most service parts shared with the GTi models

3.2 Devilbiss PRi.

| Specification |
| --- |
| Air inlet thread | ¼" Universal (M) |
| Weight | 705 gm |
| Normal working air inlet pressure at the gun | 2 bar (29 psi) |
| Air Consumption with the No. 4 Air Cap | 290 L/min (10.2cfm) |

- First class atomisation and material distribution

- Suitable for primers, filler, surfacers and polyesters

- Large spray patterns for fast and easy application

- The fit, feel, control and balance of the GTi

- Anodised gun body, stainless steel tip and needle and plated brass air cap

- High performance no.310 trans-tech compliant air cap

- Choice of 5 fluid tip sizes to suit materials and flow rates

- Paint cup includes integral filter and drip-check lid

Figure 13: Devilbiss

| Part No. | Description | Part No. | Description |
| --- | --- | --- | --- |
| 1 | Air Cap/Retaining Ring | 15 | Fluid Needle |
| 2 | Fluid Tip and Gasket | 16 | Spring |
| 3 | Gasket | 17 | Adjusting Screw |
| 4 | Baffle | 18 | Fan Adjustment Assembly |
| 5 | Lock Nut | 19 | Retaining Ring |
| 6 | Nipple | 20 | O Ring |
| 7 | Packing | 21 | Air Valve Assembly |
| 8 | Packing Gland | 22 | Snap Ring |
| 9 | Trigger Bearing Stud | 23 | Washer |
| 10 | Trigger | 24 | U Cup Seal |
| 11 | Screw | 25 | Air Valve |
| 12 | Nipple | 26 | Spring |
| 13 | Gasket | 27 | Gasket |
| 14 | Bushing |  |  |

3.3 GTi, GTiW Gravity Feed

The GTi and GTi W spray guns have been developed to take refinishers into the next millennium. They provide superb performance with all refinish paints, base coats and lacquers plus assured compliancy with EPA legislation. Developed using the world’s most advanced techniques in computational fluid dynamics the GTi has become recognized for setting the atomization, lay down and colour matching standards for compliant spray guns. The GTi W has been specially developed for the application of waterborne base coats and features a no 115 HVLP air cap and a 1.3mm fluid cap.

| Specification |
| --- |
| Air Supply Connection | Universal ¼ BSP and NPS |
| Maximum Static Inlet Pressure | P1 = 9 bar (130 psi) |
| Maximum Service Temperature | 40ºC |
| Gun Weight (with cup) | 721g |
| Air Inlet Thread | ¼" Universal (M) |
| Weight | 678 gm |
| Normal working air inlet Pressure at the Gun | 2 Bar (29 psi) |
| Air Consumption with No. 105/115 HVLP Air Cap | 453 L/min (16 cfm) |
| Air Consumption with the No. 110 Compliant/Trans-tech Air Cap | 269 L/min (9.5 cfm) |
| Materials of Construction |
| Gun Body | Anodised Aluminium |
| Nozzle | Stainless Steel |
| Needle | Stainless Steel |
| Cup | Acetal and Stainless Steel |

- First class atomization material distribution

- Reduced overspray and significant material savings

- Choice of either HVLP spray technology (No 110/115 air cap) or trans-tech technology (No 110 air cap). For base coats including waterborne metallic use the GTi with the 115 air cap and 1.3 mm fluid tip

- Transfer efficiency comfortably in excess of the EPA specified 65%

- Tough, corrosion resistant blue anodized gun body

- Accurate repeatable settings from datum markers on controls

- Wide choice of fluid tips to suit materials and preferred flow rate

- Modular components for easier faster servicing

Devilbiss

3.4 The GTi

Figure 14: The GTi

| Ref No. | Description | Part Number |
| --- | --- | --- |
| * 1 | Air Cap/Retaining Ring | GTI-407-* |
| 1a | Spring Clip | JGA-156-K5 |
| +**2 | Nozzle (up to 1.5mm) | GTI-213-**-K |
|  | Nozzle (1.6 mm to 2.2 mm) | GTI-214-**-K |
| 3 | Baffle and Seal | GTI-425-K |
|  | Baffle Seal – Kit of 5 | GTI-33-K5 |
| +4 | Packing | GTI-439-K2 |
| 5 | Spreader Valve | GTI-404-K |
| 6 | Stud and Screw | GTI-408-K5 |
| +7 | Needle (for GTI-214 Tip) | GTI-420-K |
|  | Needle (for GTI-213 Tip) | GTI-413-K |
| +8 | Spring and Pad | GTI-409-K5 |

| 9 | Bushing | GTI-420-K |
| --- | --- | --- |
| 9a | Seal Kit of 5 | JGS-72-K5 |
| 10 | Needle Adjusting Screw | GTI-414-K |
| 11 | Valve Assembly | JGK-449 |
| 12 | Trigger | GTI-108 |
| 13 | Connector | JGA-158 |
| 14 | Gun Hook | GFG-6 |
| 15 | Airflow Valve | GTI-415-K |
| 16 | ½ Ltr Gravity Cup Kit | GFC-501 |
| 17 | Cup Lid | GFC-402 |
| 18 | Drip Check Lid Kit | GFc-2-K5 |
| 19 | Filter | KGP-5 |
| 20 | Circlip | 25746-007-K5 |
| 21 | Circlip | SST-8434-K5 |
| 22 | Seal and Pin Kit (+SST-8434-K5) | GTI-428-K5 |
| 23 | Washer | GFC-17-K5 |
| 24 | Air Valve Stem Assembly |  |
| 25 | Spring | JGV-262-K5 |
| 26 | Spanner | SPN-5 |
| * Denotes Aircap Number – Available Aircaps No’s 105 and 110 ** Denotes Fluid Tip Size – Available Sizes GTI-213 0.85, 1.0, 1.1, 1.2, 1.3, 1.4, 1.5mm GTI-214 1.6, 1.8, 2.0 and 2.2mm + Parts Included in Service Kit (see accessories) |

3.5 DeVilbiss SRi/ SRi W - Spot Repair Gun

The DeVilbiss SRi/SRi W has been engineered to match sprayer’s needs for a gun with small scale control but without compromise on atomization, pattern shape, or comfort. The key to the SRi’s versatility is its spray pattern adjustment range. The fan is ideal for fade-outs and the small spot is prefect for repairs. Carry case kits are available with 2 or 3 guns. A functional tray allows up to 4 guns to be carried into the booth after filling.

Gun identification written on the side

| Specification |
| --- |
| Air supply connection | Universal ¼ BSP and NPS |
| Maximum Static Inlet Pressure | P1 = 9 bar (130 psi) |
| Nominal Gun Air Inlet Pressure with Gun Triggered | 2 bar (29 psi) |
| Maximum Service Temperature | 40ºC |
| Air Inlet Thread | ¼" |
| Gun Weight (with cup and lid) | 390g |
| Air Consumption with No. 205 HVLP Air Cap | 136 L/min (4.8 cfm) |
| Air Consumption with the No. 210 Compliant/Trans-tech Air Cap | 100 L/min (3.6 cfm) |
| Materials of Construction for Wetted Parts |
| Gun Body | Anodised Aluminium |
| Nozzle | Stainless Steel |
| Needle | Stainless Steel |
| Cup | Anti-static Nylon |
| Cup Lid | Anti-static Polypropylene |

- Fully functional, spot repair gun ergonomically styled for comfort

- Superb atomization of both solvent and water-based materials

- Choice of two compliant air caps – No. 205 (HVLP) or No. 210 (Trans-Tech)

- The natural fit feel and balance of a full size gun, provides proportionally reducing fan patterns down to spot spray

- Inexpensive, semi-disposable cups. Use 10-20 jobs and replace as required

- Cheater valve for at-the-job pressure adjustment

- Easy to clean and maintain

- Colour coded cup lids for fast material identification

Figure 15:  DeVilbiss SRi

| Ref No. | Description | Part Number |
| --- | --- | --- |
| 1 | Air Cap/Retaining Ring HVLP | SRI-407-205 |
|  | Air Cap/Retaining Ring Compliant | SRI-407-210 |
| 2 | Nozzle 0.7mm Seal, Needle (SRI-37-K) Kit | SRI-440-07-K |
|  | Nozzle 0.8mm Seal, Needle (SRI-37-K) Kit | SRI-440-08-K |
|  | Nozzle 1.0mm Seal, Needle (SRI-3-K) Kit | SRI-440-10-K |
|  | Nozzle 1.2mm Seal, Needle (SRI-3-K) Kit | SRI-440-12-K |
| 3 | Needle for 1.0 and 1.2 mm Nozzle | SRI-3-K |
|  | Needle for 0.7 and 0.8 mm Nozzle | SRI-37-K |
| 4 | Needle Spring | SRI-18-K2 |
| 5 | Needle Adjusting Knob | SRI-19-K2 |
| 6 | Spreader Valve | SRI-401-K |
| 7 | Body Bushing and Seal Kit | SRI-17-K |
| 8 | Seal | SRI-16-K5 |
| 9 | Separator | SRI-6-K5 |
| 10 | Needle Packing Kit of 3 | SRI-411-K3 |
| 11 | Air Valve Assembly | SRI-404-K |
| 12 | Air Valve Stem Assembly | - |
| 13 | Trigger Stud and Screw Kit | SRI-412-K |
| 14 | Trigger | SRI-9-K |
| 15 | Air Inlet Adaptor | SRI-20-K |
| 16 | Blanking Plug (to replace airflow valve) | SRI-21 |
| 17 | Airflow Valve | SRI-402-K |
| 18 | Spanner | SRI-50-K2 |
| 19 | Cup and Lid Kit of 2 | SRI-478-K12 |
| 20 | Aircap Seal | SRI-35-K5 |
| 21 | Air valve Spring | SRI-23-K2 |
| 22 | Air valve Seal | - |
| 23 | Retaining Ring | - |
| 24 | Lid - Kit of 6 | SRI-8-K6 |
| 25 | Air Valve Body | - |

AUTOMOTIVE REFINISHING

3.6 Pro Range of Gravity Spray Guns for Primer, Basecoat and Clearcoat

The GTi Pro Spray Guns are available marked as base or clear. The basecoat and clearcoat marking system for easy gun identification for sprayers. The ordering code for the GTIPRO spray gun is:

T2 = T2 Aircap. Alternatives are H1, T1

C   = Clearcoat Gun. Alternative is B for basecoat

13  = 13 Nozzle. Alternatives are 11,12 or 14

For the PRIPRO primer spray gun, the ordering code is:

P1  = P1 Aircap

P    = Primer Gun

16   = 16 Nozzle, alternatives 1.4, 1.8, 2.0 or 2.5

Operational Description

This GTi Pro spray gun is a professional quality gun designed with both high volume, low pressure (HVLP) technology or EPA compliant, Trans-Tech technology. The PRi Pro primer spray gun uses only Trans-Tech technology. HVLP technology reduces overspray and limits air cap pressure to 0.7 bar (10 psi). Trans-Tech complies with EPA by obtaining transfer efficiency above 65%.

Important:  These spray guns are suitable for use with both waterbased and solvent based coating materials. These guns are not designed for use with highly corrosive and/or abrasive materials and if used with such materials it must be expected that the need for cleaning and/or replacement of parts will be increased. If there is any doubt regarding the suitability of a specific material, contact your DeVilbiss distributor or DeVilbiss direct.

Note: This gun is not be used with halogenated hydrocarbon solvents or cleaning agents such as 1, 1, 1, - trichloroethane or methylene chloride. These solvents can react with the aluminum components used in this gun and cup. The reaction can become violent and lead to equipment explosion.

Figure 16: GTi Pro Spray Gun

AUTOMOTIVE REFINISHING

3.7 GTi Pro

As part of the i-system, the DeVilbiss DGi digital pressure gauge complements the GTi Pro perfectly and together with its new smooth, accurate controls, provides the professional automotive refinisher with the accuracy and precision to produce perfect, repeatable colour matches and high quality finishes first time, every time.

| Specification Air Inlet thread ¼" Universal Air Inlet Pressure 2.0 bar (29psi) Cup Capacity 560 mls Weight (Gun and Cup) 778 gms Air Cap and Ring Plated Brass Fluid Tip Stainless Steel Fluid Needle Stainless Steel |  |
| --- | --- |

3.8 In-Line Air Adjusting Value

- Lightweight at the gun pressure adjustment

- Fits neatly in-line at the gun air inlet

- Ideal for setting up compliant and HVLP spray guns

- Increase or decrease working pressure at-the-gun

- Loose swivel nut for convenient positioning

- Lightweight design (only 50 gms) does not affect balance

- 40mm diameter gauge in PSI and bar

- Calibrated up to 11 bar (160PSI)

3.9 Spray Gun Cleaning Kit

- Comprehensive range of brushes and tools

- Includes cleaning instructions and spray gun oil

- Can be hung on the mix room wall

- Handy PVC wrap format keeps tools clean

- Keep your gun in top class working order

3.10 Cup Filters

- Convenient, easy to fit suction cup paint filters

- Effectively removes dirt, flakes and scum

- Keeps the spray gun passages clear

- Inexpensive and virtually indestructible

- Resistant to most solvents - easily cleaned

- Pushes onto the fluid tube of KR suction cup

Cup Filter                                                Cup Filter Gravity Feed

Part Numbers: KR-484      51 mesh filter screen (general purpose)

KR-483      130 mesh filter screen (finer filtration)

3.11 Viscosity Cups

- The fast simple way to check out paint viscosity

- Tough, durable, easy to clean nylon

- Precision metal drain out insert

- Hanging hook for convenient storage

3.12 Duster Blow Guns

- Palm size trigger operated with diffused air flow

- Compact light weight

- Low noise factor

3.13 Spray Gun First Aid Kits

- A pack of essential spares for spray gun maintenance

- Includes necessary replacement seals and gaskets

- Lubrication oil is provide

- Relevant paint cup filter is included

- Cleaning brush provided

- Includes new trigger pivot stud and screw

- Supplied in a sturdy box for storage

3.14 Mixing Cups

- Easy to use disposable mixing cups

- Handy, disposable, easy stacking mixing cups

- Made from solvent resistant clear polypropylene

- Permanently marked with 2:1, 3:1 and 4:1 mix ratios

- Calibrated with a 0-600 volumetric measurements

Part Number:  MC-1-K50 Pack of 50 cups

3.15 Spray Gun Oil

- DeVilbiss spray gun oil

- Keep your spray gun in smooth working order

- A high quality silicone free lubricant

- 60 cc bottles with a dropper top and cover

Part Number:  SSL-10 single bottle of spray gun lubricant

3.16 SATAjet® 2000 HVLP Digital

Figure 17: SATAjet® 2000 HVLP Digital

- Nozzle set (air cap visible only)

- Self tensioning needle packing, not visible

- Trigger

- Self-tensioning air piston packing, not visible

- Stepless regulation for round and flat spray

- ColourCodeSystem

- Air connection G ¼ outside

- Air piston, not visible

- Air micrometer

- Fluid adjustment

- Material sieve, not visible

- Non-drip device

3.17 SATAjet 2000 HVLP Digital 2

Figure 18: SATAjet® 2000 HVLP Digital 2

| Part No. | Description |
| --- | --- |
| 109 | Air Connection Piece |
| 240 | Plastic Air Piston Head for SATAjet 2000 HVLP |
| 1503 | Countersunk Screw M4 x 8 DIN 965 |
| 1826 | Pack of 4 pcs , Non Drip Devices |
| 3624 | Threaded Pin |
| 3657 | Control Knob |
| 3988 | Paint Stainers, pack of 10 pcs |
| 6007 | Pack of 10 Cleaning Brushes |
| 6213 | Trigger Set for SATAjet 2000 HVLP |

| 6891 | Pack of 5 pcs. Quick Coupling Nipples G ¼ |
| --- | --- |
| 7757 | Pack of 4 CCS-Clips |
| 9653 | Tool Set |
| 10520 | Pack of 12 Springs for Paint Needle (17897) |
| 13656 | Nipple for SATA Air Coupling |
| 14985 | Battery cpl. with Compartment Lid and Sealing |
| 16162 | Swivel Complete |
| 17152 | Pack of 12 Air Piston Springs (27813) |
| 17897 | Spring for Paint Needle |
| 26500 | Pack of 12 Springs for Needle Packing (40774) |
| 26518 | Paint Flow Control Screw |
| 27813 | Spring for Air Piston |
| 33225 | Air Micrometer G ¼ outside thread |
| 40774 | Spring for Paint Needle Packing |
| 49395 | Screw-on-lid for 0.6 1 Plastic Cup |
| 52845 | Packing Screw |
| 53595 | Plastic Gravity Cup 0.61 with lid |
| 53603 | Air Micrometer cpl. |
| 55244 | Packing Set SATAjet 2000 HVLP |
| 57620 | Repair Kit SATAjet 2000 HVLP |
| 77677 | Fluid Needle Packing |
| 82552 | Air Piston Service Unit |
| 82636 | Seal Retainer, complete |
| 86843 | Air Piston Rod |
| 89771 | Spindle cpl |

4.0 Inspect and Carry out Maintenance on Air Hoses

4.1 Air Hose Construction

- There are commonly 2 types of hose material:

Rubber- very flexible and suitable for high temperatures

Plastic- cheaper and lighter

- There are 3 sizes of hoses available (6.4mm, 8.0mm, 9.5mm)

Note: All diameters are measured internally

- Air Hose (usually red or black)

- Air Hose is used to transfer compressed air from the air regulator to the gun

- Also available are male and female quick detachable fittings (QD’s) for both hoses and the interconnecting equipment

Air Hose 300 psi 20 Bar Pressure

Air Hose

4.2 Hose Construction

The air hose is a performance design combinations of 3 main components:

A.  The tube is the interior flexible artery that carries air from one end of the hose to the other.

B. The reinforcement adds strength to the hose. Its design determines pressure rating flexibility, kink and stretch and coupling retention.

C.  The cover or outer skin protects the reinforcement from oils moisture, solvents and abrasive objects.

Figure 19: Hose Construction

High Flow Fittings/Couplings

Quick Release Couplings for Air Lines

These will allow a rapid interchange of air tools and spray guns.

5.0 Calculate the Pressure Drop in an Airline

5.1 Airline Pressure Drop

This is the loss of pressure due to friction (caused by flow) between the regulator and the spray gun.

As the air travels through the hose or pipes it rubs against the walls and creates a lose of energy.

The internal diameter and the length of the hose are the biggest influence on pressure drop.

Table guide to Pressure Drop

| Hose Outlet/Gun Handle Inlet Pressure |
| --- |
| Air Hose Internal Dia. | Regulator Pressure | 5 Metre (16ft) | 10 Metre (33ft) | 15 Metre (49ft) |
| 6mm (1/4") | 3 bar (45 psi) | 1.1 bar (16 psi) | 0.8 bar (12 psi) | 0.6 bar (9 psi) |
| 6mm (1/4") | 4 bar (60 psi) | 1.7 bar (24 psi) | 1.2 bar (17 psi) | 0.9 bar (14 psi) |
| 6mm (1/4") | 5 bar (75 psi) | 2.2 bar (32 psi) | 1.7 bar (24 psi) | 1.4 bar (20 psi) |
| 6mm (1/4") | 6 bar (90 psi) | 2.7 bar (40 psi) | 2.1 bar (31 psi) | 1.7 bar (25 psi) |
| 8mm (5/16") | 3 bar (45 psi) | 1.8 bar (26 psi) | 1.5 bar (22 psi) | 1.4 bar (20 psi) |
| 8mm (5/16") | 4 bar (60 psi) | 2.5 bar (36 psi) | 2.0 bar (30 psi) | 1.9 bar (28 psi) |
| 8mm (5/16") | 5 bar (75 psi) | 3.2 bar (47 psi) | 2.7 bar (40 psi) | 2.3 bar (36 psi) |
| 8mm (5/16") | 6 bar (90 psi) | 4.0 bar (58 psi) | 3.4 bar (50 psi) | 3.2 bar (46 psi) |
| 10mm (3/8") | 3 bar (54 psi) | 1.9 bar (28 psi) | 1.9 bar (27 psi) | 1.8 bar (26 psi) |
| 10mm (3/8") | 4 bar (60 psi) | 2.7 bar (40 psi) | 2.5 bar (37 psi) | 2.3 bar (34 psi) |
| 10mm (3/8") | 5 bar (75 psi) | 3.4 bar (50 psi) | 3.3 bar (48 psi) | 3.1 bar (45 psi) |
| 10mm (3/8") | 6 bar (90 psi) | 4.3 bar (62 psi) | 4.1 bar (60 psi) | 3.8 bar (55 psi) |

6.0 Inspect and Carry Out Routine Maintenance on an Air Compressor

All air tools, spray guns, sanders, etc., must be supplied with air which is elevated to the correct pressure and volume. This is one function of air compressor. The air compressor is the major component of spray painting system.

What is an air compressor?

An air compressor is machine designed to raise the pressure of air from normal atmospheric to some higher pressure, as measured in pounds per square inch (psi).   While normal atmospheric pressure is about 14.7 pounds per square inch, a compressor will typically deliver air at pressures up to 200 psi.

Compressed air is in fact air that has been placed under pressure, forcing it to a higher pressure than the normal atmospheric pressure. Having been pressurised it will try to return to its normal state and if harnessed this can be used as a form of power.

The principal parts of a piston type compressor

- Intake

- Exhaust Valves

- Cylinder

- Crankcase

- Crankshaft

- Piston

- Connecting Rod Assembly

- Air Intake Filter

- Receiver

- Electric Motor

- On/Off Switch

- Air Valve

Figure 20: Piston Type Compressor

What types of compressors are most common in spray finishing operations?

There are two common types: the piston-type design and the diaphragm-type design. Because most commercial spray finishing operations consume large quantities of compressor air at relatively high pressures, the piston-type compressor is much more common in these situations.

How does a piston-type compressor work?

Piston-type compressor elevates the incoming air pressure through the action of a reciprocating piston. As the piston moves down, air is drawn in through an intake valve, the piston travels upward and compresses the air and then the now-compressed air is discharged through an exhaust valve to an air line. Piston compressors are available in single or multiple cylinder and single or two-stage models, depending on the volume and pressure required. This is the type of compressor usually found in a professional finishing operation.

Figure 21: Piston Compressor

How does a diaphragm-type compressor work?

This type design, which is usually quite small in volume and pressure, develops pressure through the reciprocating action of a flexible disk actuated by an eccentric.

What is a single stage compressor?

This is a piston-type compressor with one or more cylinders in which air is drawn from the atmosphere and compressed to its final pressure with a single stroke.

Where are single stage compressors used?

The application of the type is usually limited to maximum pressures of 100 psi or less. They can be used above 100psi, but they are not as efficient as two stage compressors.

What is a two stage compressor?

A compressor with two or more cylinders of unequal size in which air is compressed in two separate steps. The first or largest cylinder compresses the air to an intermediate pressure and then exhausts it into a connecting tube called an intercooler. From there the intermediate pressure air enters the smaller cylinder where it is compressed to an even higher pressure and delivered to a storage tank or the main air line.

Figure 22: Two-Stage Compressor

7.0 Type of Air Compressors

Compressed Air System

The compressed air system may be supplied from the mechanical workshop if there is sufficient capacity or, for remote body and paint shops or where capacity is too small, by a stand alone system just for the body shop. In either case it should be borne in mind that the air requirements for the body shop are somewhat different to those for a mechanical workshop. This is particularly true when considering the air supply for paint spraying.

Air for paint must be completely clean, free from moisture contamination and at the correct pressure and temperature. This is achieved by the use of regulators, various filters, condensers/driers and after coolers. Supply for air tools invariably required the addition of lubricating agent into the air. Again various types of lubricators are available from either compressor or air tool.

The exact air supply requirements are dependant upon the installation and type of compressor selected. Guidance on specific installation requirements is frequently available from compressor manufacturers, many of whom provide a full planning and installation service. Correct installation is important to ensure that air is drawn only from a clean, dry source, that the optimum air temperature is achieved and that piping is such as to prevent undue pressure or efficiency loss. Selection of compressors type will be dependant upon available budget, capacity requirements and consideration of factors such as available space, noise level requirements etc. The main features of the various types of compressor are listed below:

Piston Type

- Generally cheaper

- Noisier than rotary vane or screw types

- Less efficient than other types

Figure 23: Piston Type Compressor

Rotary Vane

- Quieter than piston type

- More compact than piston type

- More efficient than piston type

- Less moving parts

- Can be left to run continuously

- More expensive than piston type, particularly below 10hp

- Direct drive form motor provides greater mechanical efficiency

Figure 24: Rotary Vane Compressor

Screw Type

- Quieter than piston type

- More efficient than piston type

- More compact than piston type

- Usually supplied as complete system with after cooler, condenser and control system

- Direct drive from motor, provides greater mechanical efficiency

- All compressors should be serviced regularly

- All compressors should be drained daily

Figure 25: Screw Type Compressor

Air Dryer

Screw Type Compressor

Piston Type Compressor

8.0 Pressure and Volume

It is most important to understand the relationship of pressure and volume. A simple analogy is to look at a kitchen tap. If you have the tap on and place your finger against the flow you can feel the pressure. If you were to place an empty bucker under the tap what you collect in the bucket is the volume of water.

To continue the analogy if you were to use a fire hydrant the pressure of water would be similar to that of a kitchen tap but the volume of water would be considerably more. The bucket would fill much quicker with the fire hydrant.

The measurement for pressure is PSI (pounds per square inch) or bar pressure. The measurement for volume is CFM (cubic feet per minute). Air is also measured in litres per second (L/S) and cubic metres per hour (M3/H). The volume is extremely important. If the compressor being used has a maximum 4 CFM and the tool required 8 CFM then obviously it is impossible to operate the tool. It is like trying to lift a two ton weight with a one ton forklift.

If a user complains that the air receiver is running out of air and the pressure is dropping quickly he is using too large a tool for the machine’s capacity.

It is important to note that there are two different volume measurements. One is displacement which is the amount of air displaced in the compressor cylinder, the other is FAD (free air delivered) which is the actual amount of air being produced by the compressor. The FAD is a lower measurement but is the one that is used to identify the maximum performance of the compressor. The air displacement measurement should be ignored when calculating the compressor’s capacity.

Please remember your desired pressure will be achieved if you get your volume right. Once your compressor produces more volume than is required (or being used) then the air builds up to the required working pressure and stays at that pressure until the motor is switched off.

9.0 Carry Out Routine Maintenance on Air Transformers

How often should the transformer or condenser be drained of accumulated moisture and dirt?

It depends on system usage and the humidity of the air, once every day may be sufficient. In heavily used system or in humid weather the condenser or transformer should be drained more frequently.

What steps should be taken if moisture passes through the transformer or condenser?

Since moisture in the spray gun atomization air will ruin a paint job, it must be removed from the air supply. As long as the compressed air temperature is above its dew point temperature, oil or water vapour will not condense out into solid particles.

Figure 26: Air Transformer

Check the following:

- Drain transformer, air receiver and air line of accumulated moisture

- Make certain that the transformer is located at least 25 feet from the compressing outfit

- Main air line should not run adjacent to steam or hot water piping

- Compressor air intake should not be located near steam outlets or other moisture-producing areas

- Outlet on the air receiver should be near the top of the tank

- Check for damaged cylinder head or leaking head gasket. If the compressor is water cooled

- Intake air should be as cool as possible

What causes excessive pressure drop on the main line gauge of the transformer?

- The compressor is too small to deliver the required air volume and pressure

- The compressor is not functioning properly

- There is leakage in the air line or in fittings

- Valve are partially open

- The air lines or piping system is too small for the volume of air required.

9.1 Routine Compressor Maintenance

Although you should follow the manufacturer’s maintenance schedule exactly, in general all outfits require the following maintenance:

- Drain accumulated water daily more often in humid weather. It is a good idea to check it every time you drain the air transformer

- Check oil level

- Ultra sonic test receiver (tank) for weak spots

- Check release valve (danger of over pressurisation)

Danger and misuse of compressed air

- Respect pressurised air

- Never block pressurised air with your finger

- Never point pressurised air at yourself or others

- Never use it to blow dust of yours clothes

Important Notice

- Blow guns or nozzles etc. connected to air lines should not be directed at any part of the body. This is extremely dangerous practice and can result in air entering the bloodstream causing serious injury or death.

- When disconnecting an air line etc. from a quick release coupling, keep a firm grip on the flexible air line. Remember; the air begins escaping instantly and the air lines will react in a whipping action if not held firmly. This whipping action can cause serious injury.

- Please remember how dangerous compressed air can be if not handled with respect. Compressed air is a tremendous and very useful energy source, just waiting to be released at any moment in either a useful or dangerous manner.

10.0 Personal Safety

- Never work on a compressor with a necktie hanging loose, long hair hanging down or any clothing that may be sucked in by the compressor or motor.

- Never use air from a compressor for breathing purpose or filling an air cylinder unless specified or equipped for this purpose.

- Never put a ‘shut off’ valve directly in the delivery air line of a piston compressor before the receiver unless there is an adequate sized safety valve between compressor pump and ‘shut off’ valve.

- Never use non-tested flexible tube (example - garden hose) for compressed air. (Apply same caution to rigid air line).

- Never clean a machine with a blow gun without eye protection.

- Never operate a compressor without a guard. The compressor may start without warning if in auto mode.

- Never block the end of a tube, nozzle, shot gun, air line etc. with any part of the fingers or skin.

- Never start a pneumatic tool on the ground or in any position other than the intended operating position.

- Beware of pneumatic grinders/sanders etc, use all the protection available.

- Finally never, inflate a truck tyre without a wheel rim guard.

11.0 Compressed Air Pipeline Layout for Spray Room

Figure 27: Pipeline Layout for Spray Room

12.0 Spray booth operating controls and housekeeping

12.1 Use and clean a spray booth

- Spray booth operation (See Module 5 Spray Painting, unit 6 Spraying Techniques)

- A spray booth should be kept tidy at all times

- Picture demonstrates untidy floor which could be a trip hazard

13.0 Choose and Use Different Paint Drying Equipment

13.1 Waterborne Paint Air Blowing Equipment

DMG-501 & 620- Waterbased Paint Dryer System

Description

The DMG_620 Dryer System consists of a stand and 2 DMG-501 Dryer Guns (also available separately). These products have been developed for accelerated drying of waterbased paints, to reduce drying times and increase productivity.

The Dryer uses the Coanda principle, amplifying the airflow through the device from a low input of air into the handle. A replaceable filter is included to trap any airborne debris from contaminating the paint finish.

The DMG Air Dryer System complies with ATEX regulations 94/9/EC, Protection level; 2 2GX, Suitable for use in Zone 1 and 2.

| Product Specification |
| --- |
| DMG-501 Dryer Max Inlet Pressure Typical Air Consumption | 7 bar 325 litre/min @ 3.5 bar |
| DMG-520 Stand Max Inlet Pressure Hose Attachment by MPV type QD | 7 bar |

Static Electricity can be generated by air passing through hoses. To prevent such a risk, earth continuity to the equipment and the object being sprayed should be maintained. Use conductive hoses and recommended to attach an earth clamp to the stand upright. Check earth continuity with an ohmmeter, it should be less than 1 Mohm.

Never exceed the maximum recommended safe pressure for the equipment.

Never aim the dryer at anybody. It is recommended that eye protection is worn when using this equipment.

The A-weighted sound level of this product may exceed 85 dB (A) depending on the pressure/airflow being used. Details of actual noise levels are available on request. It is recommended that ear protection is worn at all times when using the equipment.

Maintenance

The only maintenance required is to ensure the equipment is kept clean and free form paint contamination.

Regularly check the filter. If the filter is blocked it will restrict the airflow and reduce the drying effect. When contaminated, dispose of the filter and use a new replacement. Filters are available in packs of 3, (Part No. DMG-5-K3)

Figure 28: Installation of Stand

| Spare Parts DMG-501-K Air Dryer |
| --- |
| 1 | Filter Pack of 3 | DMG-5-K3 |
| 2 | Male QD | MPV-5 |
| Spare Parts DMG-520-K Stand Assembly |
| 3 | Tripod Stand |  |
| 4 | Stand Upright |  |
| 5 | Clamp |  |
| 6 | Extension Arm |  |
| 7 | Hose Assembly | H-6066-B |
| 8 | Thumbscrew |  |
| 9 | Female QD | MPV-424 |

Installation

- Fit stand upright (4) to tripod base (3) and tighten thumbscrew (8).

- Slide extension arms (6) over upright (4) and secure with thumbscrew (8).

- Slide clamps (5) over the arms (6) and secure with thumbscrew (8).

- Attach hose (7) to the clamps (5).

- Insert the 2DMG dryers into the QD fitting on the clamps (5).

- Attach supply hose QD to the clamp (5) with the male QD.

The air supply should be filtered, dry and free from oil (as you supply the spraygun). The DeVilbiss range of DVFR filter/regulators are recommended.

Operation

- Turn the dryer ball valves to the off position.

- Turn on the air supply. Turn on the dryer ball valves until the required airflow is achieved. If more air is required, increase the pressure at the regulator.

Flash off of Base Coats

The paint drying and curing process is dramatically improved with the introduction of an additional air flow from the corners of the spraybooth cabin.

This clean, filtered and heated air supply creates the idea environment for the fast, controlled flash off of waterborne base-coats and rapid through curing of low VOC top coats.

The optimum air temperature together with the disruptive airflow from the whole nozzle accelerates the evaporation of water form the paint coating.

The system is designed to cover the whole vehicle in one operation which also ensures that there is consistent drying of waterborne base coats.

On the fully automatic system the built in timers, temperature control and audible alarm combine to produce the most effective quality control for operators.

This takes the guesswork out of drying and removes operator error from the flash off process.

No cooling is required at the end of flash off and the operator can immediately proceed with the next coat.

Your existing spraybooth oven can be upgraded simply and cost effectively by retrospectively installing auxiliary air moving system.

Air Blowers in Corners of Spray Booth

Figure 29: Spraybooth

- Fast flash off time 7 minutes – complete application

- High Building primer baked in just 15 minutes

- Ultra High Solids clear/solid baked in just 20 minutes

- Reduces the need for fast activators. Less stock holding

- Cover the whole vehicle

- Clean in operation

- Not compressed air driven

- Reduces energy consumption by around 40%

- Total process time for each base and clear job of 1 hour

- Adjustable nozzles for panels painted off the vehicle

- Save time & energy

- Reduces the risk of trapping water in the paint film

13.2 Infrared Drying Equipment

Drying Techniques

The basis of good work is the choice of the right tool and the right technique. For better efficiency, forced drying can also be used in substrate preparation.

Infrared and UV devices save time and money. They enable you to complete several stages of a job on the same day, ensure the fastest curing of materials and can cut energy consumption too.

Infrared drying is advantageous because it saves energy and is very efficient. The required heat is available immediately after starting and can be used exactly after starting and can be used exactly in the place where it is needed.

To avoid the most common mistakes made during infrared drying, consult the table below. It lists the most important facts.

Average Drying Times

Drying times may vary according to the kind of infrared device used. To avoid flaking and boil, use infrared drying for every coat.

| Drying Times |
| --- |
| PE-Stopper | Approx 5-7 minutes |
| Spray Filler | Approx 10-15 minutes |
| 2K-Filler (50 microns) | Approx 6-10 minutes |
| 2K-Filler (150 microns) | Approx 15 minutes |
| 2K-Topcoat | Approx 15-30 minutes |
| 2K-Clearcoat | Approx 15-30 minutes |
| The values given above serve only as examples |

In the case of critical substrates, the heat level should be reduced, which may lead to longer drying times. Base drying times for other materials on your own experience.

Infrared Drying Equipment

Control Panel

Figure 30: Infra Red Short Wave

13.3 UV Drying

UV- drying products such as UV stopper or UV filler are ideally suited for minor repairs. These products through-harden when exposed to a special UV light. The advantage of UV drying is the extremely short drying time (< 1 minute). Also, the surface does not heat up so that hardly any flash-off time is required.

14.0 Terminology & Definitions

Absolute Pressure - The existing gauge pressure plus atmospheric pressure. At sea level the gauge pressure in pounds per square inch plus 14.7 gives the absolute pressure.

Activated Alumina - A regenerative desiccant.

Aftercoolers - Devices for removing the heat of compression of the air or gas after compression is completed. They are one of the most effective means of removing moisture from compressed air.

Air Receivers - Tanks into which the compressed air or gas is discharged for the compressor. Receivers help to eliminate pulsation in the discharge line and also act as storage capacity during intervals when demand exceeds the capacity of the compressor.

Ambient Temperature - Temperature of air surrounding the equipment.

Atmospheric Pressure - The absolute pressure of the atmosphere as measured at the place under consideration.

Bar - A metric unit of pressure equal to approximately 14.5 PSIG

Booster Compressors - Machines for compressing air or gas from an initial pressure, which is considerably above atmospheric pressure to a still higher pressure.

Closed Loop System - A system in which air exhausted from the actuators is returned as a closed pressurised circuit to the compressor inlet.

Coalesce - To fuse, unite or grow into a mass large enough to fall due to gravity.

Compressor Regulator - A device fitted to the compressor to control the output of the machine.

Condensate - The liquid form from water vapour or gas into liquid.

Condensation - The process of changing vapour or gas into liquid.

Desiccant - A substance suitable for absorbing moisture.

Dew Point - The temperature at which moisture begins to condense.

- Atmospheric dew point – dew point at atmospheric pressure.

- Pressure dew point – dew point at pressure

Note: In selecting an air drying system only pressure dew point is important.

Displacement Of A Compressor Cylinder - The volume swept through by the piston. This is usually expressed in cubic per minute.

Double-Acting Compressors - In which compression takes place on both strokes per revolution in each compressing element.

Dryers, Refrigerated - Dryers that use a refrigeration system to cool and condense moisture.

Dryers, Regenerative - Dryers that use two desiccant towers. One tower dries the incoming air while the other regenerates the desiccant.

Filter - A device which removes foreign matter from the working medium.

Fusible Plug - A device fitted in the hot discharge zone of a compressor for protection against high temperature.

Gauge Pressure - The pressure as measured with reference to atmospheric pressure; where no other indication is given, pressure expressed ‘bar’ are assumed to be gauge pressure.

Hot Gas By-Pass Valve - A valve that by-passes hot refrigerant gas from high pressure to the low pressure side of a refrigerant system. The valve is generally used to reduce refrigeration capacity to maintain a desired refrigerant temperature.

Intercoolers - Devices for removing the heat of compression of air or gas between consecutive stages of multi-stage compressors.

Lubricator - Device which introduces a controlled quantity of lubricant into the working medium.

Moisture Separators - Devices for collecting and removing moisture precipitated from the air or gas during the process of cooling.

Micron - One millionth of one meter or 1 meter = 1,000,000 microns.

Multi-Stage Compressors or Compound Compressors - Are those in which compression from initial to final pressure is completed in two or more distinct steps or stages.

Portable Compressors – Consisting of a compressor and driver mounted so that they are readily moved as a unit.

Pressure Regulator (Pressing Reducing Valve) - A device which reduces the line pressure and maintains it relatively constant despite changes in inlet pressure and outlet flow rate.

Pressure Relief Valve (Safety Valve) - A device which limits the maximum system pressure by exhausting the compressed air to atmosphere when the required back pressure is exceeded.

PSIG - Pounds per square inch pressure as measured by a gauge.

Purge - Usually refers to the removal of unwanted air, water or gas.

Refrigerant - A fluid used for heat transfer in a refrigeration unit. Feron 22 and R134A are commonly used refrigerants.

Regeneration - Reactivation of desiccant.

Ring Main - An air main which begins and ends at the compressor so that every outlet has two possible sources (routes) of supply.

Saturated Air - Air at 100% relative humidity. It takes 7.8 cu.ft. of free air to saturate compressed air at 100 PSIG. Therefore, as long as the atmospheric relative humidity is over 12.9% (7.8 x 12.9 = 100%), which it almost is, the compressed air from an air compressor is saturated. (This also explains why an air dryer is a must for a compressed air system).

SCFM – Standard Cubic Feet per Minute. Standard air is defined at 68oF (20oC), 14.7  PSIA (1.01 bar) and 36% relative humidity (density, 0.0750 lbs./cu.ft).

Silica Gel - A regenerative desiccant.

Single-Acting Compressors - Are those in which compression takes place on but one stroke per revolution in each compressing element.

Single-Stage Compressors - Are those in which compression from initial to final pressure is complete in single step or stage.

Specific Energy Consumption - The general accepted method of measuring the efficiency of air compressor i.e. the amount of KW or HP required to produce 100 CFM (FAD) at full load.

Two-Stage Compressors - Are those in which compression from initial to final pressure is completed in two distinct steps or stages.

Vacuum Pumps - Machines for compressing air or gas from an initial pressure which is below atmospheric to final pressure which is near atmospheric.

Volumetric Efficiency - The ratio of the actual capacity of the compressor to displacement and is expressed in per cent.

15.0 Compressed Air Pipeline Layout for Work Shop

Figure 31: Compressed Air Pipeline Layout

Summary

The selection, use and maintenance of refinishing equipment, spray guns, cups, compressors, regulators, hoses, spray booths, respirators, etc. is very important for creating a perfect finish. It definitely requires a solid knowledge of surface preparation, finishes and spray painting equipment; the first two are extensively covered. But even an extensive knowledge of surface preparation techniques and paint chemistry is not enough to assure a professional finish. It must still be applied by a spray gun and all of the variables of its use must be controlled.

The equipment necessary to apply the finish – the spray gun, cup, regulator, hoses, compressor etc. – must all be matched to the job and to each other and the equipment must be used and maintained properly, with an appreciation of how it works the way it does.

The moment of truth for any finish is when the trigger is pulled on the gun!

Self Assessment

Questions – Module 5. Unit 2

1.   What is the function of the second stage of a two stage compressor?

2.  Explain F.A.D

3.   How often should you drain off water from a compressor?

4.   Explain the term H.V.L.P.

5.  What is a spray gun?

6.   Explain a gun set up.

7.   At what pressure does a SRI W operate?

8.   Why must compressed air never be directed at anyone?

9.   What pressure should a spray booth work at?

10.  Which method dries paint faster – Infra red or ultra violet?

Answers to Questions 1-10. Module 5. Unit 2

1.

Compress the air to a lighter pressure.

2.

Free air delivery

3.

Once a day

4.

High volume low pressure

5.

A spray gun is a tool that uses compressed air to atomize paint and other materials and apply it to a surface.

6.

Air cap, Fluid Tip, Fluid Needle

7.

29 psi or 2 bar

8.

It can result in air entering the blood stream causing serious injury or death.

9.

Negative and Neutral

10.

Ultra violent

Suggested Exercise

Strip and reassemble a suction fed sprat gun. Identify and explain the function of the different parts.

Operate and shut down a spray booth.

Outline a routine maintenance schedule for the following: a spray booth, an air transformer and compressor.

Training Resources

- Classroom/workshop

- Spray booth and mixing room

- Gravity and suction feed spray guns

- Compressor

- Air transformer

- Air hoses

- Visual aids

27-33 Upper Baggot Street
Dublin 4