TRADE OF PLASTERING

PHASE 2

Module 1

SLABBING, RENDERING, FLOATING AND SKIMMING

UNIT: 10

Fixing Angle and Stop Beads

Produced by

In cooperation with subject matter expert:

Terry Egan

Some images & text courtesy of Gypsum Industries Ltd.

© SOLAS

Table of Contents

Introduction	1

Unit Objective	1

1.0	Identify the Function of Angle Beads and Stop Beads	1

1.1	Beads for Plaster and Plasterboard	1

2.0	Interpret and Draw Circles	8

2.1	Construction of Basic Circles	8

3.0	Estimate Correctly the Linear Quantities of Materials Required	10

3.1	Linear Quantities of Beading and Costings	10

3.2	Calculation of Perimeters	11

# Introduction

Welcome to this section of your course which is designed to introduce you the learner, to angle beads, stop beads, circles and quantities.

# Unit Objective

By the end of this unit each apprentice will be able to:

- Identify the function of angle beads and stop beads

- Interpret and draw circles

- Estimate correctly the quantities of materials required

# 1.0	Identify the Function of Angle Beads and Stop Beads

### Key Learning Points

- Beads for plaster and plasterboard

## 1.1	Beads for Plaster and Plasterboard

### Plaster Beads for Internal Use

Angle Bead

Plaster Thickness: 13mm	Lengths: 2400/2700/3000

Provides a true, straight corner which protects and reinforces plaster where it is most vulnerable. One size adjusts for thickness.

Plaster Stop Bead

Plaster thickness: 10/13/16/19mm	Lengths: 2400/3000

Finishes and reinforces plaster edges and it comes in various thicknesses.

Movement Bead and Corner Movement Bead

Movement Bead	Corner Movement Bead

Plaster Thickness: 13mm	Lengths: 3000

Movement Bead forms movement joints in plaster and render. It allows for up to ±3mm movement. Corner Movement Bead allows up to 6mm movement in both planes.

### Plaster Beads for Thin-Coat Plaster

Thin-Coat Angle Bead and Thin-Coat Stop Bead

Thin Coat Angle Bead	Thin-Coat Stop Bead

Plaster Thickness: 3mm	Lengths: 2400/2700 (Angle Bead only)/3000

For 3mm plaster finishes on plasterboard or any smooth background.

Thin-Coat Expanded Small-Mesh Wing angle Bead

Plaster Thickness: 3mm	Lengths: 2400/3000

The expanded mesh wings provide a key for thin-coat plaster corners.

### Beads for Dry-Lining

Dry Wall Corner Bead

Plaster Thickness: 2mm	Lengths: 2400/3000

For steel protection on plaster board corners.

Plasterboard Edging Bead

Plaster Board Thickness: 12.5mm	Lengths: 3000

A reversible, dual-purpose bead which reinforces plasterboard edges by enclosing them in a protective steel section.

### Beads for External Use

Angle Bead (Standard Wing)

Plaster Thickness: 16/20mm	Lengths: 3000

For external render work. One size for both thicknesses.

Angle Bead and Stop Bead

Angle Bead	Stop Bead	Stop Bead

Render	20mm	10mm	13mm
Thickness

Length 3000 (all)

The Angle Bead protects render corners. The Stop Bead Finished and protects render edges.

External Render Stop (Standard Wing) and External Stop Type 2

External Render Stop (Standard Wing)	External Stop Type 2

Render	16/20mm		20mm
Thickness

Lengths 3000

Forms and protects lower edge of render.

Movement Bead

Render Thickness: 21mm	Lengths: 3000

Forms movement joints in render and allows for up to ±3mm movement.

### Metal Lathing

Expanded Metal Lathing (internal use)	Riblath (external use)

| Material Thickness | Nominal Weight kg/m2 | Mesh Size SW (mm) | Maximum fixing Centres (mm) |
| --- | --- | --- | --- |
| 0.500 | 1.11 | 9 | 300 |
| 0.725 | 1.61 | 9 | 350 |
| 0.400 | 0.90 | 9 | 300 |

| Material Thickness | Nominal Weight kg/m2 | Rib Depth (mm) | Maximum Centres of support (mm) |
| --- | --- | --- | --- |
| 0.3 | 1.16 | 8 | 600 |
| 0.5 | 1.61 | 8 | 600 |

Expanded Metal Lathing serves as a key for lightweight plasters over small openings, carrier for lightweight plaster finishes on walls and ceilings and general plaster reinforcement.

Riblath is a stainless steel carrier for all rendered finishes. A pre-galvanised carrier of render should only be used in sheltered / moderate exposure away from the coast.

# 2.0	Interpret and Draw Circles

### Key Learning Points

- Construction of basic circle

## 2.1	Construction of Basic Circles

Parts of a Circle

Diameter is a straight line drawn across a circle and passing through its centre.

Radius is a straight line drawn from the centre of a circle to its circumference.  It is equal to half its diameter.

Tangent is a straight line which touches the circumference or arc of a circle.

Arc is a section of the circumference of a circle.

An important mathematical constant is used when solving area and perimeter calculations of a circle. This constant is called ‘Pi’ and is represented by the symbol π.  The numerical value of the constant is 3.142 and is the number of times that the diameter of the circle will go into the circumference length of the same circle.  This constant applies to all circles, whatever their size.

The area of a circle is calculated using the formula πr²:

Area of a circle	=	π  x  r²

where π	=	3.142

r	=	radius of circle

Note: To square a figure you have to multiply it by itself, ie:

4²	=	4 x 4

4²	=	16

Therefore, the surface area of a circle:

=	π  x  r²

=	π  x  radius  x radius

### Overview

The area of a circle is calculated using the formula:

Area of circle = π  x  r²

Where π = 3.142 and r = radius

r² means radius x radius

### Example 1

Find the area of a circle with radius 2m:

Area of circle	=	π r²

=	π x r x r

=	3.142 x 2 x 2

=	12.568m²

### Example 2

Find the area of a circle with diameter 3m.

Remember to halve the diameter to find the radius.

Area of circle	=	π r²

=	π x r x r

=	3.142 x 1.5 x 1.5

=	7.0695m²

# 3.0	Estimate Correctly the Linear Quantities of Materials Required

### Key Learning Point

- Linear quantities of beading and costings

- Linear quantities of perimeters

## 3.1	Linear Quantities of Beading and Costings

This is the system used for measuring items within the trade that cannot be measured in square metres. With these items, all that can be measured is their length.

Some of these items are: Angles and angle beads and coving.

Narrow widths of plastering (normally 300mm in width).

If a length of beading 2 metres long cost €10.00; find the cost of length 35cm in length.

2m	= 200mm

1cm will cost 10.00÷200	= €0.05

35cm will cost 0.05x35	= €1.75

## 3.2	Calculation of Perimeters

Find the Area and Perimeter of Figure 2?

Find the Area and Perimeter of Figure 3?

Answer

Area = 66cm², Perimeter = 58cm.

Area = 66cm², Perimeter = 42cm

27-33 Upper Baggot Street
Dublin 4