| Trade of Sheet Metalwork |
| --- |
| Module 3: | Thermal Processes |
| Unit 10: | MMA Welding Depositing Straight Weld Runs |
|  | Phase 2 |

Table of Contents

List of Figures	6

List of Tables	7

Document Release History	8

Module 3 – Thermal Processes	9

Unit 10 – MMA Welding Depositing Straight Weld Runs	9

Learning Outcome:	9

Key Learning Points:	9

Training Resources:	10

Key Learning Points Code:	10

Layout of Typical Plant	12

Equipment	14

The Manual Metal Arc Process	15

Manual Metal Arc Welding Equipment	17

Types of Joints	18

Welding Positions	22

Welding Symbols	24

New Welding Symbols	28

Terminology	33

Angle of Bevel	34

Arc Length	34

Tack Weld	35

Types of Run	35

Heat Affected Zone	36

Penetration	36

Advantages of D.C. Welding	38

Types of Welding Plant	39

Direct Current (d.c.)	39

Alternating Current (a.c.)	40

Effect of Short Circuiting	40

Electrodes	41

Functions of the Electrode Coating	41

Types of Electrode Coating	42

Welding Current	42

Electrodes	43

American Welding Society (AWS) Classification System for Electrodes	44

Mild Steel Electrodes	44

First and Second Digits	44

Third and Fourth Digits	44

The Arc	45

To Strike the Arc	45

Removing the Electrode	46

Welding Techniques	48

Current Too Low	48

Current Too High	48

Correct Current	48

Arc Length	48

Speed of Travel	49

Angle of Electrode	49

Distortion	50

Longitudinal Distortion	50

Transverse Distortion	50

Angular Distortion	51

Control of Distortion	52

Expansion and Contraction in Welding and Cutting Processes	52

Safety	54

Remember	54

First Aid	57

Preparation for Welding	58

Safety in Manual Arc Welding	59

Equipment	59

Eye Protection	60

Recommended Filters	60

Screening and Protective Clothing	60

Weld Defects and their Causes	61

Lack of Penetration	61

Lack of Fusion	61

Porosity	61

Slag Inclusion	61

Undercut	61

Overlays	62

Cracking	62

Blowholes	62

Burn Through	62

Excessive Penetration	62

Common Weld Faults	63

Weld Variations	64

Arc Too Short	64

Arc Too Long	64

Travel Too Slow	65

Travel Too Fast	65

Current Too Low	66

Current Too High	66

Correct Run	67

Manual Metal-Arc Welding	68

Reinforcement (building up)	68

Reinforcing in Flat Position	68

Hard Facing	69

Tack Welds	69

Self Assessment	70

Answers to Questions 1-7. Module 3.Unit 10	73

Bibliography	76

Index	77

# List of Figures

Figure 1 - M.M.A. Welding - Reinforcement (Build Up)	11

Figure 2 - Layout of Typical Plant	12

Figure 3 - Manual Metal-Arc Welding Process	16

Figure 4 - Welding Symbol Location 1	26

Figure 5 - Welding Symbol Location 2	26

Figure 6 - Method of Representation	28

Figure 7 - Intermittent Weld	29

Figure 8 - Angle of Bevel	34

Figure 9 - Arc Length	34

Figure 10 - Tack Weld	35

Figure 11 - Types of  Run	35

Figure 12 - Heat Affected Zone	36

Figure 13 – Penetration	36

Figure 14 - Functions of the Electrode Coating	41

Figure 15 – Electrodes	43

Figure 16 - Angle of Electrode	49

Figure 17 - Longitudinal Distortion	50

Figure 18 - Transverse Distortion	50

Figure 19 - Angular Distortion	51

Figure 20 - Arc Too Short	64

Figure 21 - Arc Too High	64

Figure 22 - Travel Too Slow	65

Figure 23 - Travel Too Fast	65

Figure 24 - Current Too Low	66

Figure 25 - Current Too High	66

Figure 26 - Correct Run	67

# List of Tables

Table 1 - Welding Symbols	25

Table 2 - Elementary Symbols	29

Table 3 - Types of Electrode Coating	42

Table 4 - Current to Use when Welding Mild Steel Plate	42

Table 5 -Electrodes	43

Table 6- Recommended Filters	60

Table 7 - Common Weld Faults	63

# Document Release History

| Date | Version | Comments |
| --- | --- | --- |
| 27/09/06 | First draft |  |
| 09/01/07 | Implemented edits from Brendan Deasy. |  |
| 07/04/14 | 2.0 | SOLAS transfer |

# Module 3 – Thermal Processes

## Unit 10 – MMA Welding Depositing Straight Weld Runs

Duration – 7 Hours

### Learning Outcome:

By the end of this unit each apprentice will be able to:

Select electrode type and size

Adjust power source to the required setting

Identify and state precautions and regulations

Strike and maintain arc, deposit a series of beads on 8 mm plate to form reinforced pads

Identify surface weld defects

### Key Learning Points:

| Sc Rk | Ancillary equipment – proper earthing and connections. |
| --- | --- |
| Rk | Welding terms. |
| Rk | Types of weld and weld symbols. |
| Rk | Electrodes – types, sizes, flux coating, function of flux. |
| Rk Sk | Arc striking, arc gap, maintaining arc, electrode angle. |
| Rk Sk | Welding technique – speed of travel – amperage/current control. |
| H Rk | Distortion causes and correction. |
| H Rk | Safety precautions – hazards. |
| H Rk | Protective clothing – skin and eye protection. |
| Rk | Identification of surface defects – causes and correction. |
| Sc | Basic electricity. AC/DE sources. |

### Training Resources:

MMA welding power source

Figure 1 and hand-outs

3.2 rutile electrodes

Safety clothing and ancillary equipment

200 x 150 x 8 mm mild steel plate

### Key Learning Points Code:

M = Maths	           D= Drawing     RK = Related Knowledge Sc = Science

P = Personal Skills	Sk = Skill	   H = Hazards

Figure 1 - M.M.A. Welding - Reinforcement (Build Up)

# Layout of Typical Plant

Figure 2 - Layout of Typical Plant

- Wall Switch (Isolator)

- Connecting Cable

- Welding Set

- Welding Cable

- Electrode Holder

- Welding Electrode

- Return (earth) lead

- Current regulator (fine)

- Current regulator (coarse)

Write the answers to these questions in your notebook.

You may refer back in the notes if necessary.

- Write down the correct names of the following in your notebook.

A. B. G. E. D.

# Equipment

Welding plant

Earth clamp

Electrode holder.

# The Manual Metal Arc Process

When two wires which form part of an electrical circuit are brought together and then pulled slowly apart, an electric spark is produced across their ends.

This spark, or arc as it is called, has a temperature of up to 3,600°C. As the arc is confined to a very small area it can melt metal almost instantly.

If one of these wires is connected to the job and the other to a wire rod or electrode, as it is usually called, the heat of the arc melts both the metal of the job and the point of the electrode. The molten metal from the electrode mixes with that from the job and forms the weld. It is important to realise that tiny globules of the molten metal from the electrode are forced through the arc (they do not fall by gravity). If this were not so it would be impossible to use this process for overhead welding.

Figure 3 - Manual Metal-Arc Welding Process

# Manual Metal Arc Welding Equipment

To create the arc discussed earlier it is necessary to have a voltage to drive the current (which supplies the required heat) through the circuit. A voltage of between 60 and 100 V is required to create the arc, but once it has been obtained only 20-40 V are required to maintain it.

The following stages occur when creating an arc:

With the welding plant switched on, and before welding commences, no current passes through the leads and the ammeter reads zero. A voltage has been applied to the circuit, however, and the voltmeter will read the open-circuit or no-load voltage (i.e. between 60 and 100 V).

When the electrode is brought into contact with the job a large current, called the short-circuit current, passes through the leads, and the ammeter will deflect a large amount. While this is happening, however, the voltage drops almost to nothing. The tip of the electrode becomes hot because of the resistance created between it and the job.

If the electrode is slightly withdrawn an arc is formed between the electrode and the job. The air between the two conducts the welding current. As the arc is formed the voltage rises to between 20 and 40 V and the current falls to the value to which it has been set (i.e. the welding current).

The arc is then in the normal welding condition. The heat generated by the arc melts both the workpiece and the electrode, and metal is deposited in the weld pool. During the depositing of the weld metal, variations in both the voltage and current of the arc can occur and the welding plant must be capable of coping with these changes.

# Types of Joints

Fillet

Square Butt

Single Vee Butt

Double Vee Butt

Single U Butt

Double U Butt

Single Bevel Butt

Double Bevel Butt

A. Single J Butt

B. Double J Butt

Corner Joint

Single Vee Butt

T Joint

Double Vee Butt Joint

Lap Joint

# Welding Positions

Overhead

Inclined

Flat

Horizontal Vertical

Vertical

# Welding Symbols

The basic requirements of the British standard BS499 schedule of symbols for welding comprise of:

- A symbol for the type of welded joint.

- An arrow, elbow and reference line to indicate the position of the weld.

- The addition of weld details where necessary.

- Symbols for supplementary instructions.

| Type of Weld | Symbol |
| --- | --- |
| Single Fillet |  |
| Double Fillet |  |
| Square Edge Butt |  |
| Single ‘Vee’ Butt |  |
| Double ‘Vee’ Butt |  |
| Single Bevel Butt |  |
| Double Bevel Butt |  |
| Single ‘U’ Butt |  |
| Double ‘U’ Butt |  |
| Single ‘J’ Butt |  |
| Double ‘J’ Butt |  |
| Edge |  |
| Seal |  |
| Sealing Run |  |
| Weld All Round |  |
| Weld on Site |  |
| Backing Bar |  |
| Flush Finish |  |
| Spot |  |
| Radiograph |  |

Table 1 - Welding Symbols

The symbols for the different types of welds are applied to drawings in the following manner.

If the welding symbol is placed above the arrow line as shown on the left in Figure 4 it means that the weld should be made from the other side of the joint as shown on the right in Figure 4 and not the side to which the arrow is pointing.

Figure 4 - Welding Symbol Location 1

Where the welding symbol is placed below the arrow line, as shown on the left in Figure 5 this means that the weld should be made on the side of the joint indicated by the arrow as shown on the right in Figure 5.

Figure 5 - Welding Symbol Location 2

If the weld symbol is placed on both sides of the arrow line, this means that the joint should be welded from both sides.

Write the answers to these questions in your notebook.

You may refer back in the notes if necessary.

- What do the following symbols signify?

Note: A lot of these symbols have now been updated and are listed in the following pages. It is important to be aware of the older symbols as they will be on old drawings which may still be in use.

For all up to the minute weld symbols see ISO2553 Third Edition on Welded Joints/Seams.

# New Welding Symbols

Figure 6 - Method of Representation

The various categories of joints are characterized by a symbol which in general is similar to the shape of the weld to be made.

The symbol shall not be taken to prejudge the process to be employed.

The elementary symbols are shown in Table 2.

If the joint should not be specified but only be represented that the joint will be welded, brazed or soldered, the following symbol shall be used.

| No. | Designation | Illustration | Symbol |
| --- | --- | --- | --- |
| 2. | Square butt weld |  |  |
| 3. | Single-V butt weld |  |  |
| 10. | Fillet weld |  |  |
| 12. | Spot weld |  |  |

Table 2 - Elementary Symbols

Figure 7 - Intermittent Weld

# Terminology

A 	Toe

B 	Root

A	Throat Thickness

This is the shortest 			distance from the root 		to the surface of the 			deposit.

A	Leg Length

B	Leg Length

This is the distance 			from the root to the 			toe of a weld 				measured along the 			weld face.

## Angle of Bevel

The angle of an edge which is cut or chamfered.

Figure 8 - Angle of Bevel

## Arc Length

The distance between the tip of the electrode and the surface of the weld pool.

Figure 9 - Arc Length

## Tack Weld

A short weld used in assembly to hold the work-pieces in position during welding, usually ¼˝- ½˝ long.

Figure 10 - Tack Weld

## Types of Run

- Root Runs
The first runs deposited in the root of a joint where there is more than one run.

- Filler Runs
The build up runs between root and capping runs.

- Capping or Final Runs
The weld runs which make up the top layer of the joint.

- Sealing Run
A weld deposited on the root side of a weld after completion of the main weld.

Figure 11 - Types of  Run

## Heat Affected Zone

In this area, the parent metal has a change in mechanical properties due to the heat from welding, but it has not been melted.

Figure 12 - Heat Affected Zone

## Penetration

This is the depth the molten metal from the electrode penetrates the parent metal.

Figure 13 – Penetration

Write the answers to these questions in your notebook.

You may refer back in the notes if necessary.

- What is throat thickness?

- What is leg length?

- Where is the toe of a weld?

- What is arc length?

- What is the top weld run called?

- What is the name of a weld deposited on the root side of a weld after completing the main weld?

# Advantages of D.C. Welding

- Allows welding of non-ferrous metals.

- It’s portable.

- Deposits a smoother weld.

- It’s safer in damp conditions.

- Reverse polarity available ⅓ or ⅔ heat option.

# Types of Welding Plant

## Direct Current (d.c.)

With this system the current passes in one direction only. The heat generated is split into two parts, two-thirds goes to the positive pole and one-third to the negative pole. This is important as it determines the design of the electrode to be used.

If a light-coated electrode is connected to the positive terminal it quickly becomes too hot to use for welding. But if the workpiece is connected to the positive terminal and the electrode to the negative terminal, the weld pool becomes the hottest part and the electrode stays beneath its critical heat value.

The polarity of the electrode, when using d.c. for welding, is most important and the electrode manufacturer's recommendations should be strictly adhered to, except in exceptional circumstances where the work must be kept as cool as possible. The terms used by British Standards for electrodes state that:

Electrodes connected to the positive terminal are called electrode positive, and electrodes connected to the negative terminal are called electrode negative.

Basic equipment -

- A generator driven either from d.c. mains (motor generator) or by a petrol or diesel engine;

- An a.c./d.c. motor generator set; or

- Rectifying equipment.

The generator must supply an open-circuit voltage of about 60 V which will drop to approximately 20 V when the arc is struck. Generators can be obtained with various current ratings from 100 to 600 A, and the modern types automatically adjust themselves to allow for the voltage fluctuations of the arc. Normally only one welder can work from a set.

## Alternating Current (a.c.)

With a.c., the direction of the current flow continually changes. This reverse in direction takes place 50 times per second. Because of this reversal of the current flow the two poles are maintained at the same temperature, and reversal of the terminals has no effect as is the case with d.c.

The a.c. plant consists of a transformer which will reduce the supply voltage down to the required open-circuit voltage, i.e. 60 100 V. Various types of set are available giving different current ranges. Depending on the set, current values from 20 A up to 500 A can be obtained.

Alternating-current welding plant is cheaper to .buy than the equivalent direct current set, requires less maintenance, is quieter in operation, and the running costs are ,lower: The use of a.c. equipment is dependent upon an a.c. supply being available, and therefore when welding on sites it is not usually possible and a d.c. engine-driven generator is used.

### Effect of Short Circuiting

When the welder strikes his arc the welding generator is subjected to a short circuit and the current passing through the windings of the generator increases. If this increase in current is not controlled the windings will overheat, resulting in damage to the generator. In most cases this short-circuit current should not exceed 150% of the normal welding current and overload devices are fitted to protect the equipment.

# Electrodes

## Functions of the Electrode Coating

The six main functions of the electrode coating are as follows:

- To act as a flux and remove the impurities from the surfaces being welded.

- To form a slag over the weld, this does the following: protects the molten metal from contact with the air; slows down the cooling rate of the weld, helping to prevent brittleness of the weld; and provides a smoother surface by preventing ripples caused during the welding process.

- It forms a neutral gas atmosphere, which helps to protect the molten weld pool from oxygen and nitrogen in the surrounding air.

- It helps to stabilise the arc, allowing a.c. to be used.

- It can add certain constituents to the weld by replacing any lost during the welding process.

- It can speed up the welding process by increasing the speed of melting of the metal and the electrode.

Figure 14 - Functions of the Electrode Coating

## Types of Electrode Coating

Table 3 - Types of Electrode Coating

## Welding Current

Table 4 shows the approximate current to use when welding mild steel plate. It is important that the manufacturer’s instructions regarding the particular electrode being used are refer to.

Table 4 - Current to Use when Welding Mild Steel Plate

## Electrodes

When a piece of metal is heated in the atmosphere it combines with the oxygen and nitrogen to form oxides and nitrides which combine with the metal. If these were allowed to form in the weld it would result in poor quality, weak and brittle weld.

It is therefore necessary to protect the weld area from the air. This can be done either by surrounding the weld area by an inert gas or by the use of suitable fluxes.

It is usual, with manual metal arc welding, to use coated electrodes. These electrodes consist of a metal core surrounded by a layer of suitable flux coating.

Figure 15 – Electrodes

| Electrical Conditions for Electrodes | Welding Positions |
| --- | --- |
| These are indicated as follows: D+ = direct current with electrode positive D- = direct current with electrode negative D± = direct current with electrode positive or negative A.C. = alternating current | Approved welding positions for an electrode are indicated as: H = horizontal F = flat V = vertical D = downband O = overhead |

Table 5 -Electrodes

## American Welding Society (AWS) Classification System for Electrodes

### Mild Steel Electrodes

The method of classifying of electrodes is based on the use of a four-digit number, preceded by the letter 'E' for 'Electrode'.

The first two digits designate the minimum tensile strength of the weld metal (in 1,000 psi) in the as-welded condition.

The third digit indicates the position in which the electrode is capable of making satisfactory welds.

The fourth digit indicates the current to be used, and the type of flux coating.

For example, the classification of E6012 electrodes is derived as follows:

E 601 2 = Metal arc welding electrode.

E 601 2 = Weld metal UTS 60,000 psi min.

E 601 2 = Usable in all positions.

E 601 2 = Rutile type coating: AC or DC negative.

The detail of the classification is shown below:

### First and Second Digits

E 60xx 	As-welded deposit, UTS 60.000 psi min. for E 6010, E 6011, E 6012, E 6013, E 6020, E 6027 UTS.

E 70xx 	As-welded deposit, UTS 70.000 psi min. for E 7014, 7015, 7016, 7018, E 7024 and E 7028.

### Third and Fourth Digits

The third and fourth digits indicate positional usability and flux coating types e.g.

Exx10	High cellulose coating, bonded with sodium silicate.
Deeply penetrating, forceful, spray-type arc. Thin, friable slag. All-positional. DC electrode positive only.

Exx11 	Very similar to Exx10, but bonded with potassium silicate to permit use on AC or DC positive.

Exx12	High rutile coating, bonded with sodium silicate. Quiet are, medium penetration. all-position at. AC or DC negative.

# The Arc

## To Strike the Arc

- Lower your welding shield.

- Point the electrode downwards and away from the body at an angle of 65° - 80° to the plate surface.

- Lower the electrode holder until the electrode striking end is about 25mm away from the position at which the weld deposit is about to start.

- Strike the electrode against the plate and immediately withdraw it slightly to make the welding arc.

Electric current supplied from a power source passes through a welding lead and the electrode. The electrode is held a short distance from the workpiece and as the current jumps from the electrode to the workpiece a hot and brilliant arc is formed. The arc is formed before metal is transferred.

## Removing the Electrode

To free an electrode stuck to the workpiece:

Jerk the electrode up and sideways away from the workpiece.

If this fails to free the electrode, open the electrode holder and move the holder away.

Keep your shield on. If possible switch off welding machine.

Remove the electrode with a pliers or hammer and chisel.

Do not touch electrode with bare hand.

Write the answers to these questions in your notebook.

You may refer back in the notes if necessary.

- At what angle should the electrode be to the workpiece when striking the arc?

- What is the first thing to do before attempting to strike an arc?

- Give two ways of removing an electrode which has stuck to the workpiece.

# Welding Techniques

## Current Too Low

If the current value is too low the resulting weld has poor penetration, due to the lack of heating to create complete fusion. The weld filler metal tends to heap up on the surface of the plate without fusing to it and the arc has an unsteady sputtering sound.

## Current Too High

When the current value used is too high the electrode becomes red hot and a large amount of spatter takes place. This can result in blowholes being formed in the plate, excessive penetration resulting in weld metal beads on the underside of the plate, undercut along the edge of the weld and excessive oxidation and slag which is hard to remove. The arc has a fierce crackling sound.

## Correct Current

With the correct current the arc has a steady crackling sound. The weld formed has good penetration and is easily controlled.

## Arc Length

The arc length is the distance between the tip of the electrode and the surface of the weld pool. It should be approximately equal to the diameter of the wire core of the electrode being used. When this distance is correct the electrode metal is deposited in a steady stream of metal particles into the weld pool. If the arc length is reduced it becomes difficult to maintain the arc, due to the increase in welding current that takes place, and it can result in the electrode becoming welded to the weld pool. Also, if the arc length is increased the welding current is reduced, resulting in a poor weld being produced, and the protective gas shield produced from the electrode surrounding the weld pool cannot efficiently prohibit the formation of oxides, etc., in the weld.

## Speed of Travel

A fast rate of travel results in a thin deposit of the filler metal and can result in insufficient fusion of the filler metal with the base metal. The surface of the weld has elongated ripples and a porous crater.

Too slow a rate of travel gives a wide thick deposit of the filler and it can allow the slag to flood the weld pool making it difficult to deposit the filler metal. The surface of the weld appears as coarse ripples and has a flat crater.

# Angle of Electrode

Figure 16 - Angle of Electrode

When the weld is completed with the correct current, arc length, speed of travel and electrode angle, the deposit will be of regular thickness and width and the surface will have even, smooth ripples, and be free from slag entrapment and porosity.

# Distortion

## Longitudinal Distortion

If a weld is made on one side of a flat strip of thin plate, the plate will bend upwards as it cools.

Figure 17 - Longitudinal Distortion

## Transverse Distortion

When a butt weld is made between two thin plates that are free to move, the plate edges will be drawn together. The edges in advance of the weld may overlap.

Put a series of tack welds along the joint to prevent distortion.

Figure 18 - Transverse Distortion

## Angular Distortion

If a fillet weld is deposited between two plates in a T-joint, the angle between the plots will be reduced as the weld cools.

Figure 19 - Angular Distortion

# Control of Distortion

## Expansion and Contraction in Welding and Cutting Processes

As has been seen earlier, when a piece of metal is heated it expands and, on cooling down, contracts. With welding and cutting processes the heating takes place over a localized area of the metal and expansion can only take place in that portion of the metal. The subsequent contraction that takes place on cooling can result in forces causing distortion or, even worse, cracking of the metal. When a weld bead is deposited on the joint between two plates, the molten metal passing through the arc is at a very high temperature. The arc melting the edges of the joint and the filler and base metal fuse together. As the arc moves across the joint the deposited bead starts to cool and considerable contraction forces are set up in the weld area.

As the deposited metal was at a higher temperature than the parent metal it will contract more and also, since its volume is greater, there is a large volume of metal shrinkage. The result is distortion of the joint. The following are several ways of controlling the effect of distortion during welding: (a) presetting; (b) backstepping or stepwelding; (c) jigging; (d) preheating. They are described below.

- Presetting entails setting the joint out of alignment prior to welding so that after contraction has taken place the joint is aligned.

- Backstepping or stepwelding entails welding the joint in short steps, ensuring that expansion and contraction zones are placed next to one another.

- Jigging entails holding the metal being welded in a jig, restraining the distortion mechanically.

- Preheating entails heating the metal to be welded prior to welding, and has the effect of allowing equal contraction to take place in both the weld and parent metal.

When the weld is made with a large number of small runs the distortion is greater.

To control the distortion the following points should be remembered:

- Design
Remove distortion by using: 
(a) Minimum number of joints.
(b) Easily reached joints.
(c) Correct weld size for the strength required.
(d) Welds balanced about material axis.

- Parent metal
		
When welding is balanced heat input is balanced, thus eliminating angular distortion.
Reduce distortion by using: 
(a) Correct weld sequence.
(b) Correct deposition technique which ensures minimum heat input.

- Joint preparation
Reduce distortion by using: 
(a) Smallest included angle possible.
(b) Smallest root gap possible.
(c) Double-sided preparation when parent metal is thicker than 5/8˝.

# Safety

## Remember

Welding rays are very dangerous. Always wear a welding shield.

Always wear safety clothes as welding produces sparks and hot metal.

Always wear goggles when chipping slag as it will be hot and sharp.

Always screen your welding from other trainees to avoid risk of radiation.

Never weld enclosed tanks without consulting your instructor as there is a risk of explosion.

Always examine welding cables for damage and report faults to your instructor immediately.

## First Aid

Always notify your instructor if you get grit in your eye.

Don’t try to remove it yourself.

Use an eye bath and eye lotion to wash eyes if you get “flash” or “arc eye”.

Repeat this every four hours.

# Preparation for Welding

- Make sure that outer clothing is free from oil, grease or flammable material.

- Protect your arms from exposure to arc rays.

- Cuffs on overalls and turn-ups on trousers are lodging places for sparks, try to cover them up.

- Ensure that the welding shield contains the correct filter glass and that it is not cracked or damaged.

# Safety in Manual Arc Welding

## Equipment

The power supply for arc welding may be either a.c. or d.c. The voltages used are in the order of up to 100 V and currents of up to 600 A. It is therefore essential that adequate precautions are observed to protect both the operator and other personnel in the area from the risks associated with electricity. The following points should be observed when using arc welding equipment.

- Make sure that the welding circuit is correctly earthed.

- The welding cables should be adequately insulated. Never use damaged cables.
(See illustration 'A').

- Ensure that the welding cables are free from kinks and that they do not become crushed or pinched under heavy loads. (See illustration 'B').

- Check that the power source is disconnected from the supply before attaching cables to the terminals.

- Always use a fully insulated electrode holder when welding in confined spaces, or where it is difficult to get access to the weld without touching the surrounding metal (See illustration 'C').

# Eye Protection

It is essential to protect the eyes and face from the arc. The use of a face mask or head shield with the correct filter glass is essential.

# Recommended Filters

| Shade (B.S. 679) | Metal Arc Current |
| --- | --- |
| 9 EW | Up to 100 A |
| 11 EW | 100-300 A |
| 13 EW | Over 300 A |

Table 6- Recommended Filters

# Screening and Protective Clothing

Adequate screening around the welding area should be erected to protect the workers in the immediate vicinity. The operator should also be protected from the splashing metal and sparks given off the welding by wearing a leather apron, spats and gloves. When working on a site or in damp conditions the use of rubber-soled boots is also advisable.

Note: Be careful welding containers which had previously contained inflammable material.

# Weld Defects and their Causes

## Lack of Penetration

Lack of penetration is the failure of the filler metal to penetrate into the joint. It is caused by:

Incorrect edge penetration

Incorrect welding technique

Inadequate de-slagging

## Lack of Fusion

Lack of fusion is the failure of the filler metal to fuse with the parent metal. It is caused by:

Insufficient heat

Too fast a travel

Incorrect welding technique

## Porosity

Porosity is a group of small holes throughout the weld metal. It is caused by the trapping of gas during the welding process, due to chemicals in the metal, dampness, or too rapid cooling of the weld.

## Slag Inclusion

Slag inclusion is the entrapment of slag or other impurities in the weld. It is caused by the slag from previous runs not being cleaned away, or insufficient cleaning and preparation of the base metal before welding commences.

## Undercut

Undercuts are grooves or slots along the edges of the weld caused by:

Too fast a travel

Too great a heat build-up

Bad welding technique

## Overlays

Overlays consist of metal that has flowed on to the parent metal without fusing with it. The defect is caused by:

Insufficient heat

Contamination of the surface of the parent metal

Bad welding technique

## Cracking

Cracking is the formation of cracks either in the weld metal or the parent metal. It is caused by:

Bad welding technique

Unsuitable parent metals used in the weld

## Blowholes

Blowholes are large holes in the weld caused by:

Gas being trapped, due to moisture

Contamination of either the filler or parent metals

## Burn Through

Burn through is the collapse of the weld pool due to:

Poor edge preparation

Too great a heat concentration

## Excessive Penetration

Excessive penetration is where the weld metal protrudes through the root of the weld. It is caused by:

Too big a heat concentration

Too slow a travel

Incorrect edge preparation

# Common Weld Faults

When you first start to weld you will find that you have some defects in the welds. These are explained here with their causes.

| Defect | Cause |
| --- | --- |
| Uneven Welds | Moving the torch along the joint too quickly or slowly, zig zaging movements not the same. |
| Fused portion not in joint but to one side | Not playing the torch over the joint equally at each side. |
| Holes in the joint | Holding the flame too long in one place and overheating the metal. |
| Oxide inclusions | Not cleaning the base metals (metal being welded) properly before starting. Inclusions will be seen as black specks on the surface of broken welds. |
| Adhesions | Not enough heat to one side of a joint or welding speed too high. As a result the weld metal will break clearly from the metal surface on one side. |
| Overheating | Moving flame too slowly. |

Table 7 - Common Weld Faults

# Weld Variations

## Arc Too Short

Ripples irregular in height and width.

Figure 20 - Arc Too Short

## Arc Too Long

Coarse ripples evenly spaced. Crater flat and blistered.

Figure 21 - Arc Too High

## Travel Too Slow

Coarse ripples evenly spaced. Crater flat.

Figure 22 - Travel Too Slow

## Travel Too Fast

Elongated ripples. Crater porous.

Figure 23 - Travel Too Fast

## Current Too Low

Irregular ripples with slag trapped in valleys. Crater irregular.

Figure 24 - Current Too Low

## Current Too High

Coarse ripples evenly spaced. Crater hollow.

Figure 25 - Current Too High

## Correct Run

Smooth ripples evenly spaced. Crater sound.

Figure 26 - Correct Run

# Manual Metal-Arc Welding

## Reinforcement (building up)

This is the process of adding to or building up the thickness of a section by depositing metal on the surface. If the deposited metal has wear-resistant properties it is known as hard facing.

| Material | ½˝ (12.5 mm) mild steel, 1 off, min. 6˝ (15.0 cm) x 8˝ (20.0 cm) |
| --- | --- |
| Preparation | Clean surface |
| Electrode | 8 s.w.g. (4.0 mm) Class 2 |
| Current | 150-170 amperes |

### Reinforcing in Flat Position

Example Procedure EP8

- Deposit a straight run near the edge of the plate about 6" (15.0 cm.) long.

- Deposit second run alongside directing the electrode at about 60° into the angle formed by the toe of the first run and the plate surface.

- Maintain the angle of 65° - 75° to the surface of the plate in the direction of travel.

- Use weaving technique carrying the electrode end over one-third of the width of the first run.

- If correctly deposited the second run will be built up to the height of the first run and a flat junction obtained.

- Deposit the third and subsequent runs in a similar way to the second, alongside and fusing into its preceding run.

- Continue deposition until the pad of metal is about 4" (10.0 cm.) wide.

Visual Examination

Cool and saw through the reinforced section and plate, and visually examine the cross-section.

A correctly deposited reinforcement should be free from marked valleys or ridges at the junctions between the runs. There should be no trapped slag, and the deposit should be free from porosity.

### Hard Facing

Example Procedure EP9

(This is an optional procedure)

- The type of electrode chosen should be one that has similar operating technique to that of a Class 2 electrode, i.e. an electrode with a tutile type covering.

- Repeat the deposition as for EP8.

- Turn the plate through 90° and deposit the second layer with runs transverse to the runs of the first layer.
Note that in hard facing procedure it is usually necessary to deposit at least two layers in order to achieve full hardness. The hardness of the first layer will be affected by dilution with the parent metal.

| Material | ½˝ (12.5 mm) mild steel, 1 off, min. 6˝ (15.0 cm) x 8˝ (20.0 cm) |
| --- | --- |
| Preparation | Clean surface |
| Electrode | 8 s.w.g. (4.0 mm) hard facing type (not tubular) |
| Current | Mean recommended value for the electrode |

Visual Examination

Repeat the visual examination as for EP8 provided the deposit is not too hard to saw.

If desired make a series of hardness tests on the surface of the deposit after preparing a small flat area with a file and smooth emery paper.

A wide range in hardness readings indicates variation in alloy content of deposit. This can be caused by excessive arc length or by grove variation in arc length during deposition.

## Tack Welds

A tack weld is a short weld used to help assemble and to maintain the position of parts during welding.

Tack welds should be between three and four times the plate thickness, up to a maximum length of 1 ½ ˝ (3.0 mm.) at the ends of the joint.

For intermediate tack welds the length should be between two and three times the plate thickness, up to a maximum length of 1 ½ ˝ (35.0 mm).

# Self Assessment

Questions on Background Notes – Module 3.Unit 10

1.     If your weld has irregular ripples in height and width, what is wrong?

2.    If your weld has coarse ripples evenly spaced and a flat crater, what is wrong?

3.    If your travel is too fast, how does this affect your weld?

4.    What happens if the current is to high?

5.     What is undercut? Give two causes of undercut.

6.    What is porosity? Give two causes of porosity.

7.    What is lack of fusion? Give one cause of lack of fusion.

# Answers to Questions 1-7. Module 3.Unit 10

1.

The current is too low resulting in poor penetration. The weld filler metal tends to heap up on the surface of the plate.

2.

The current is too high. The electrode becomes too hot and a large amount of splatter takes place, this can result in blowholes forming in the plate, excessive penetration results in weld metal beads on the underside of the plate. The arc has a fierce cracking sound.

3.

A fast rate of travel results in a thin deposit of the filler metal and can result in insufficient fusion of the filler metal with the base metal. The surface of the weld has elongated ripples and a porous crater.

4.

Weld appearance has coarse ripples evenly spaced and a hollow crater. Weld may suffer from excessive penetration undercut. Also see Answer 2.

5.

Undercuts are groves or slots along the edges of the weld caused by: Too fast a travel rate. Too great a heat build-up. Bad welding technique.

6.

Porosity is a group of small holes throughout the weld metal caused by: a. The trapping of gas during the welding process b. Chemicals in the metal. c. Dampness d. Too rapid cooling of the weld.

7.

Lack of fusion is the failure of the filler metal to fuse with the parent metal caused by: Insufficient heat. Too fast a rate of travel. Incorrect welding techniques.

# Bibliography

Notes:

International Standard				ISO2553

Third Edition on Welded Joints/Seams

# Index

A

Advantages of D.C. Welding, 38

Alternating Current (a.c.)

Effects of Short Circuiting, 40

American Welding Society (AWS) Classification System for Electrodes

First and Second Digits, 44

Mild Steel Electrodes, 44

Third and Fourth Digits, 44

Angle of Electrode, 49

C

Common Weld Faults, 63

Control of Distortion, 52

Expansion and Contraction in Welding and Cutting Processes, 52

D

Distortion, 50

Angular Distortion, 51

Longitudinal Distortion, 50

Transverse Distortion, 50

E

Electrodes, 41

American Welding Society (AWS) Classification System for Electrodes, 44

Electrodes, 43

Functions of the Electrode Coating, 41

Types of Electrode Coating, 42

Welding Current, 42

Equipment, 14

Eye Protection, 60

L

Layout of Typical Plant, 12

M

Manual Metal Arc Welding Equipment, 17

Manual Metal-Arc Welding, 68

Reinforcement (building up), 68

Tack Welds, 69

N

New Welding Symbols, 28

P

Preparation for Welding, 58

R

Recommended Filters, 60

Reinforcement (building up)

Hard Facing, 69

Reinforcing in Flat Position, 68

S

Safety, 54

First Aid, 57

Remember, 54

Safety in Manual Arc Welding, 59

Equipment, 59

Screening and Protective Clothing, 60

Self Assessment, 70

T

Terminology, 33

Angle of Bevel, 34

Arc Length, 34

Heat Affected Zone, 36

Penetration, 36

Tack Weld, 35

Types of Run, 35

The Arc, 45

Removing the Electrode, 46

To Strike the Arc, 45

The Manual Metal Arc Process, 15

Types of Joints, 18

Types of Welding Plant, 39

Alternating Current (a.c.), 40

Direct Current (d.c.), 39

W

Weld Defects and their Causes, 61

Blowholes, 62

Burn Through, 62

Cracking, 62

Excessive Penetration, 62

Lack of Fusion, 61

Lack of Penetration, 61

Overlays, 62

Porosity, 61

Slag Inclusion, 61

Undercut, 61

Weld Variations, 64

Arc Too Long, 64

Arc Too Short, 64

Correct Run, 67

Current Too High, 66

Current Too Low, 66

Travel Too Fast, 65

Travel Too Slow, 65

Welding Positions, 22

Welding Symbols, 24

Welding Techniques, 48

Arc Length, 48

Correct Current, 48

Current Too High, 48

Current Too Low, 48

Speed of Travel, 49